Thermoplastic Industrial Hoses

THE ASSOCIATION FOR HOSEAND ACCESSORIES DISTRIBUTION

TIGERFLEX™ ISO 9001 QUALITY M.S.

EDITION 0218

2001™ Series Hose	10

2020™ Series Hose	12

AMPH™ Amphibian™ Series Hose	22

BARK™ “Bark Hose” Series Hose	33

BCCF™ Banding Coils	56

BCRT™ Banding Coils	56

BCWF™ Banding Coils	56

BW™ “Blue Water” Series Hose	40

CF™ Cold Flex™ Series Hose	41

CG™/CG-SL™ “Cover Guard” Series Hose	37

F™ Tiger™ Suction Series Hose	39

FMCR™ “Spa Hose” Series Hose	47

FT™ Series Hose	17

G™ Tiger™ Suction Series Hose	39

GC-C™ “Ground Cover” Series Hose	31

GT™ Series Hose	36

GTF™ Series Hose	18

GTFE™ Series Hose	18

GTG™ Series Hose	36

H™ Series Hose	38

J™ Series Hose	38

K™ Series Hose	38

LK™ Lawn King™ Series Hose	34

LKC™ Lawn King™ Series Hose	34

MH™ “Marine Hose” Series Hose	46

MILK™ Series Hose	16

MILK-LT™ Series Hose	16

MULCH™ Series Hose	32

MULCH-LT™ Series Hose	32

ORV™ Series Hose	54

OV™ Oil Vac™ Series Hose	55

PF™ Plas-T-Flow™ Series Hose	27

S™ Tiger™ Suction Series Hose	39

SBDC™ TigerClamps™	58

SBDCR™ TigerClamps™	58

SH™ Series Hose	43

SLV-DRP™ Banding Sleeves	57

SLV-VAP™ Banding Sleeves	57

SLV-VLT™ Banding Sleeves	57

STIG™ Series Hose.......................N...E..W 	52

TBLU™ Tiger™ Blue Series Hose	50

TG™ Tiger™ Green Series Hose	48

TR1™ Tiger™ Series Hose	20

THT™ Tiger™ Series Hose	21

TRED™ Tiger™ Red Series Hose	50

TSD™ Tiger™ Series Hose	51

TY™ Tiger™ Yellow Series Hose	49

UBK™ Series Hose	25

UF1™ Ureflex™ Series Hose	24

UF2™ Ureflex™ Series Hose	23

UFC™ Ureflex™ Series Hose	26

UV1™ Urevac™ Series Hose	35

UVE™ Urevac™ Series Hose ..........N...E..W 	35

UV2™ Urevac™ Series Hose	29

UV3™ Urevac™ Series Hose	28

UVF™ Series Hose	19

UVPE™ Series Hose	30

VLT-SD™ Voltbuster™ Series Hose	13

VOLT™ Voltbuster™ Series Hose	11

W™ Series Hose	42

WBS™ Series Hose	14

WE™ Series Hose	9

WG™ Series Hose	45

WH™ Series Hose	43

WOR™ Series Hose	53

WST™ Series Hose	44

WSTF™ Series Hose	15

WT™ Series Hose	8

Index of Reference Pages

Application Guide	6-7

Care and Maintenance	64

Cautionary Statement and Limited Warranty	Back Cover

Chemical Resistance Guides and Warning	67-73

Compliance Footnotes for Tigerflex™ Catalog Products	62

Effect of Temperature on Working Pressure & Vacuum Ratings	66

EPDM Chemical Resistance Guide	72

Features and Advantages Catalog Icon Guide	4

Features and Advantages Guide by Hose Series	5

Flexibility	63

Index of Products by Series	2

Index of Reference Pages	2

Kuriyama Value™	75

PVC and Polyurethane Resistance Guide	68-71

Quality Assurance	62

Recommended Practices	64

SBR Chemical Resistance Guide	73

Storage and Handling	65

Table of Contents	3

Tigerflex™ Accessories Compatability Chart	59-61

Tigerflex™ Products Custom Inquiry Form	74

Working Pressure Ratings	66

Index of Products by Series

NOTE: Although every effort has been made to accurately show the color of the Tigerflex™ hoses in this catalog, because of the limitations of four-color process printing some of the colors shown herein may not be exact.

# Table of Contents

Index of Products by Series	2

Index of Reference Pages	2

Table of Contents	3

Features and Advantages Catalog Icon Guide	4

Features and Advantages Guide by Hose Series	5

Application Guide	6-7

Liquid Suction:

H™ Series Hose	38

J™ Series Hose	38

K™ Series Hose	38

Tiger™ Suction F™ Series Hose	39

Lawn King™ LK™ Series Hose	34

Lawn King™ LKC™ Series Hose	34

Urevac™ UV1™/UVE™ Series Hose	35

GT™ Series Hose	36

GTG™ Series Hose	36

“Cover Guard” CG™/CG-SL™ Series Hose	37

Ducting:

Tiger™ TR1™ Series Hose	20

Tiger™ THT™ Series Hose	21

Amphibian™ AMPH™ Series Hose	22

Ureflex™ UF2™ Series Hose	23

Ureflex™ UF1™ Series Hose	24

UBK™ Series Hose	25

Ureflex™ UFC™ Series Hose	26

Urevac™ UV3™ Series Hose	28

Urevac™ UV2™ Series Hose	29

UVPE™ Series Hose	30

“Ground Cover” GC™ Series Hose	31

“Ground Cover” GC-C™ Series Hose	31

MULCH™ Series Hose	32

MULCH-LT™ Series Hose	32

“Bark Hose” BARK™ Series Hose	33

STIG™ Series Hose............................N..E..W 	52

Material Handling:

WT™ Series Hose	8

WE™ Series Hose	9

2001™ Series Hose	10

Voltbuster™ VOLT™ Series Hose	11

2020™ Series Hose	12

Voltbuster™ VLT-SD™ Series Hose	13

WBS™ Series Hose	14

WSTF™ Series Hose	15

MILK™ Series Hose	16

MILK-LT™ Series Hose	16

FT™ Series Hose	17

GTF™ Series Hose	18

GTFE™ Series Hose	18

UVF™ Series Hose	19

Plas-T-Flow™ PF™ Series Hose	27

Food Grade:

Tiger™ Suction G™ Series Hose	39

Tiger™ Suction S™ Series Hose	39

“Blue Water” BW™ Series Hose	40

Coldflex™ CF™ Series Hose	41

W™ Series Hose	42

WH™ Series Hose	43

SH™ Series Hose	43

WST™ Series Hose	44

WG™ Series Hose	45

“Marine Hose” MH™ Series Hose	46

“Spa Hose” FMCR™ Series Hose	47

Tiger™ Green TG™ Series Hose	48

Tiger™ Yellow TY™ Series Hose	49

Tiger™ Red TRED™ Series Hose	50

Tiger™ Blue TBLU™ Series Hose	50

Tiger™ TSD™ Series Hose	51

WOR™ Series Hose	53

ORV™ Series Hose	54

Oil Vac™ OV™ Series Hose	55

Accessories:

Banding Coils	56

Banding Sleeves	57

TigerClamps™	58

Tigerflex™ Accessories Compatability Chart	59-61

References:

Quality Assurance	62

Compliance Footnotes for Tigerflex™ Catalog Products	62

Flexibility	63

Care and Maintenance	64

Recommended Practices	64

Storage and Handling	65

Effect of Temperature on Working Pressure & Vacuum Ratings	66

Working Pressure Ratings	66

Chemical Resistance Guides and Warning	67

PVC and Polyurethane Resistance Guide	68-71

EPDM Chemical Resistance Guide	72

SBR Chemical Resistance Guide	73

Tigerflex™ Products Custom Inquiry Form	74

Kuriyama Value™	75

Cautionary Statement and Limited Warranty	Back Cover

The trademarks contained in this publication are trademarks of Kuriyama of America, Inc.

NOTE: Although every effort has been made to accurately show the color of the Tigerflex™ hoses in this catalog, because of the limitations of four-color process printing some of the colors shown herein may not be exact.

The “Tigerflex” design trademarks contained in this publication are trademarks of Tigers Polymer Corporation.

Features & Advantages Catalog Icon Guide

Abrasion Resistant – Indicates hoses designed to help resist internal wear caused by the transfer of abrasive materials.

Abrasion Resistant Plus – Indicates hoses designed to help resist internal wear caused by the transfer of highly abrasive materials.

“Cold-Flex” Materials – Indicates hoses formulated to remain flexible in sub-zero temperatures.

Easy Slide – Indicates hoses with an external rigid helix designed to slide easily over rough surfaces. Easy-to-handle.

Food Grade – Indicates hoses which comply with applicable FDA requirements for food contact. Several of these hoses also meet USDA and 3-A requirements.

Oil Resistant – Indicates hoses which exhibit resistance to animal and petroleum based oils.

Static Dissipative – Indicates hoses formulated with static dis- sipative compounds or hoses containing a grounding wire to help prevent the build-up of static electricity.

Transparent Construction – Indicates hoses with a transparent or semi- transparent tube. These hoses allow the user visual confirmation of material flow, and the ability to see if material or condensation has collected in the hose tube.

Water – Indicates hoses which can be used for freshwater and saltwater transfer.

Features & Advantages Guide By Hose Series

| Food Grade: |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2001 |  | X |  |  | X | X | X | X |  |
| 2020 |  | X | X | X | X | X | X | X |  |
| FT |  |  |  |  | X |  |  | X | X |
| GTF |  |  |  | X | X |  |  | X | X |
| GTFE |  |  |  | X | X |  | X | X | X |
| MILK |  |  |  |  | X |  |  | X | X |
| MILK-LT |  |  | X |  | X |  |  | X | X |
| PF |  | X | X | X |  | X | X | X |  |
| UVF | X |  | X | X | X | X |  | X |  |
| VOLT/VLT-SD |  | X | X | X | X | X | X | X |  |
| WBS | X |  |  |  | X |  | X | X | X |
| WE | X |  |  |  | X |  | X | X | X |
| WSTF |  |  |  | X | X |  |  | X | X |
| WT | X |  |  |  | X |  |  | X | X |
| Material Handling: |  |  |  |  |  |  |  |  |  |
| AMPH |  | X | X |  |  | X | X |  | X |
| BARK | X |  |  | X |  |  |  | X | X |
| GC-C | X |  | X |  |  | X |  | X |  |
| MULCH | X |  |  |  |  |  |  | X | X |
| MULCH-LT | X |  | X |  |  |  |  | X | X |
| STIG |  | X | X |  |  | X | X |  |  |
| TR1 |  | X | X |  |  |  | X |  | X |
| THT | X |  | X | X |  |  | X |  | X |
| UBK |  | X | X | X |  | X | X |  |  |
| UF1 |  | X | X |  |  | X | X |  |  |
| UF2 |  | X | X |  |  | X | X |  |  |
| UFC |  | X | X |  |  | X | X | X |  |
| UV-2 | X |  | X | X |  | X | X | X |  |
| UV-3 |  | X | X | X |  | X | X | X |  |
| UVPE | X |  | X |  |  | X | X | X |  |
| Ducting: |  |  |  |  |  |  |  |  |  |
| CG/CG-SL |  |  |  | X |  |  |  | X | X |
| GT |  |  |  | X |  |  |  | X | X |
| GTG |  |  |  | X |  |  |  |  | X |
| LK | X |  | X | X |  |  |  |  | X |
| LKC | X |  | X | X |  |  |  | X | X |
| UV1/UVE | X |  | X | X |  | X | X | X |  |
| Liquid Suction: |  |  |  |  |  |  |  |  |  |
| BW |  |  | X |  |  |  |  | X | X |
| CF | X |  | X |  |  |  | X |  | X |
| F/G/S |  |  |  |  |  |  |  | X | X |
| H/J/K |  |  |  |  |  |  |  | X | X |
| MH |  |  |  |  |  |  |  |  | X |
| ORV |  |  |  |  |  | X |  |  | X |
| OV |  | X | X |  |  | X |  | X |  |
| SPA |  |  |  |  |  |  |  |  | X |
| TG/TY/TRED/TBLU |  |  | X | X |  |  |  |  | X |
| TSD |  |  | X | X |  |  |  |  | X |
| W |  |  | X |  |  |  |  | X | X |
| WG |  |  |  |  |  |  |  |  | X |
| WH/SH |  |  | X |  |  |  |  | X | X |
| WOR |  |  |  |  |  | X |  |  | X |
| WST |  |  |  |  |  |  |  | X | X |

NOTE: For details regarding the features & advantages listed, refer to the catalog page for each product.

✚ = Primary Applications

✔ = Secondary Applications

Food Grade

Material Handling

Application Guide

|  | 2001 | 2020 | FT | GTF/ GT FE | MILK/ MILK- LT | PF | UVF | VLT- SD | VOLT | WBS | WE | WSTF | WT | AMPH | BARK | GC- C | MULCH/ MULCH- LT | STIG | TR1 | THT | UBK | UF1 | UF2 | UFC | UV2 | UV3 | UVPE |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Agricultural dry fertilizers Agricultural liquid fertilizers Agri-foam systems |  |  |  |  |  |  |  |  |  |  |  |  |  | ✚ |  |  |  |  |  | ✚ | ✚ | ✚ |  | ✚ | ✚ |  |  |
| Air seeder lines Bulk truck and railcar unloading Cable and hose bundle protection | ✔ | ✚ |  |  |  | ✚ |  | ✚ | ✚ |  | ✔ |  | ✔ | ✚ |  |  |  | ✔ | ✔ |  | ✚ | ✚ ✔ | ✔ | ✚ | ✚ |  |  |
| Concrete resurfacing dust collection Drain lines Ducting, ventilation & fume removal |  |  |  | ✚ |  |  | ✚ |  |  |  |  |  | ✔ |  |  |  |  |  |  | ✔ ✔ |  |  |  |  | ✔ |  |  |
| Dust collection Fish suction Fly ash collection |  |  |  | ✔ |  |  | ✚ |  | ✚ |  |  | ✔ |  | ✚ |  |  |  | ✚ | ✚ | ✔ ✚ | ✚ | ✚ | ✚ |  | ✚ | ✚ |  |
| Food grade blower and ducting systems Food grade liquids - water, beer, wine and juice Food grade material handling - heavy duty abrasive | ✚ | ✚ | ✚ | ✚ | ✚ |  | ✚ | ✚ | ✚ | ✔ | ✔ | ✚ | ✚ ✔ |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Food grade material handling - standard duty Gold dredging Hydro excavation | ✔ | ✔ | ✔ | ✔ |  |  | ✔ | ✔ | ✔ | ✚ | ✚ | ✚ | ✚ | ✚ |  |  | ✔ |  | ✚ | ✚ |  |  |  |  |  |  |  |
| Ice transfer Industrial vacuum equipment Insulation blowing | ✔ | ✔ | ✚ | ✔ | ✚ |  |  | ✚ | ✚ | ✔ | ✔ | ✚ | ✔ ✔ | ✚ |  |  |  | ✚ | ✚ | ✚ | ✚ | ✚ | ✚ | ✚ | ✔ | ✔ ✔ | ✔ |
| Irrigation lines Lawn and leaf collection Liquid manure handling |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ✚ | ✔ | ✔ |  |  |  |  |  |  |  |  |  |  |
| Marine bilge discharge Marine plumbing Material chutes | ✔ | ✔ |  | ✔ |  | ✔ | ✔ | ✚ | ✚ | ✔ | ✔ |  | ✔ | ✔ |  |  |  | ✚ | ✔ | ✚ | ✔ | ✚ | ✚ | ✚ | ✚ | ✔ | ✔ |
| Material handling - heavy duty abrasive Material handling - standard duty Material handling - light duty | ✚ ✔ | ✚ ✔ | ✔ | ✔ ✚ |  | ✚ | ✔ ✔ | ✚ ✔ | ✚ ✔ | ✔ ✚ ✔ | ✔ ✚ ✔ |  | ✔ ✚ ✔ | ✚ ✔ | ✚ | ✚ ✚ | ✚ | ✚ ✔ | ✚ ✚ | ✔ ✚ ✔ | ✚ ✔ | ✚ ✔ | ✚ ✔ | ✚ ✔ | ✔ ✚ | ✚ ✔ | ✚ ✚ |
| Milk and dairy product transfer Milling machine scrap recovery Mining applications (MSHA) |  |  | ✚ |  | ✚ | ✚ |  | ✚ | ✚ |  |  |  |  | ✚ |  |  |  | ✚ | ✚ | ✚ | ✚ | ✚ | ✚ | ✚ |  | ✚ | ✔ |
| Mulch, bark, wood chips, other surfacing materials Oil skimming Oil sluries |  |  |  |  |  |  |  |  |  |  |  |  |  | ✔ | ✚ | ✚ | ✚ |  |  |  |  |  |  |  |  |  |  |
| Oil suction Pharmaceutical product transfer Plastic processing equipment | ✚ ✚ | ✔ ✔ | ✔ | ✚ ✔ |  | ✔ ✚ | ✚ ✔ | ✔ ✚ | ✔ ✚ ✚ | ✚ ✚ | ✚ ✚ | ✔ | ✚ ✚ | ✔ |  |  |  | ✔ |  |  | ✔ ✔ | ✔ ✔ | ✔ | ✔ ✚ | ✔ | ✔ ✚ | ✔ ✚ |
| Pneumatic conveying systems Poultry processing Pumps, rental and construction dewatering | ✚ |  | ✔ ✚ |  | ✔ |  |  | ✚ | ✚ | ✚ | ✚ |  | ✚ ✚ |  |  |  |  |  |  | ✔ |  |  |  |  |  |  |  |
| Pumps, trash Recreational vehicle (RV) pluming Rock dusting |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ✔ |  |  |  |  |  |  |  |
| Rock, gravel, sand and crushed concrete vacuuming Septic and wastewater handling Sewer truck boom hose |  |  |  |  |  | ✔ |  |  |  |  |  |  |  | ✚ ✚ |  |  |  | ✚ ✔ | ✚ ✚ | ✚ ✔ ✚ | ✚ ✔ | ✚ ✔ | ✚ ✔ |  |  | ✔ | ✔ |
| Shot blast recovery Slurry handling Soil, seed and compost delivery |  |  |  |  |  |  |  |  |  |  |  |  |  | ✚ ✚ | ✚ | ✚ | ✚ | ✚ | ✚ ✚ | ✚ | ✚ | ✚ | ✚ | ✚ |  | ✔ |  |
| Spa, pool and hot tub pluming Suction and discharge Wand hose |  | ✚ |  |  |  |  |  | ✚ |  |  |  | ✚ |  |  | ✔ |  |  |  | ✚ |  | ✔ |  |  |  | ✚ |  |  |
| Water suction - heavy duty Water suction - standard duty |  |  | ✚ ✔ |  | ✚ |  |  |  |  | ✔ |  | ✚ ✔ | ✔ | ✔ |  |  |  | ✔ | ✔ |  |  |  | ✔ |  |  |  |  |

CAUTION NOTE: This application guide provides information on typical hose applications. Actual results may vary due to variances in the operating conditions involving temperature, chemical resistance, working pressure, etc. Please refer to the specifications printed for each product in this catalog, along with information regarding chemical resistance and our Cautionary Statement, to better insure successful results.

✚ = Primary Applications

✔ = Secondary Applications

Ducting	Liquid Suction

|  | CG/ CG-SL | GT/ GTG | LK/ LKC | UV1/ UVE | BW | CF | F/G/S | H/J/K | MH | OV | SPA | TG/TY/ TRED/ TBLU | TSD | W | WG | WH/ SH | WOR/ ORV | WST |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Agricultural dry fertilizers Agricultural liquid fertilizers Agri-foam systems |  |  |  |  | ✔ | ✔ ✔ ✔ | ✔ ✔ ✔ | ✔ ✚ ✔ |  |  |  | ✚ ✔ | ✚ ✚ | ✔ | ✔ |  |  |  |
| Air seeder lines Bulk truck and railcar unloading Cable and hose bundle protection | ✚ | ✔ | ✔ |  |  | ✔ | ✔ | ✚ |  |  |  |  |  |  |  | ✔ |  |  |
| Concrete resurfacing dust collection Drain lines Ducting, ventilation & fume removal | ✔ ✔ | ✚ ✚ | ✔ | ✚ ✚ | ✔ |  | ✔ | ✚ | ✚ |  | ✚ |  |  | ✔ | ✔ | ✚ |  |  |
| Dust collection Fish suction Fly ash collection | ✔ | ✚ | ✚ | ✚ | ✔ |  |  |  |  |  |  |  |  | ✚ | ✚ | ✚ |  | ✚ |
| Food grade blower and ducting systems Food grade liquids - water, beer, wine and juice Food grade material handling - heavy duty abrasive |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Food grade material handling - standard duty Gold dredging Hydro excavation |  |  |  |  | ✔ |  |  |  |  |  |  |  |  | ✚ | ✚ | ✚ |  | ✔ |
| Ice transfer Industrial vacuum equipment Insulation blowing |  | ✔ |  | ✚ | ✔ | ✔ |  |  |  |  |  |  |  | ✔ ✔ | ✔ | ✔ |  |  |
| Irrigation lines Lawn and leaf collection Liquid manure handling |  | ✔ | ✚ | ✔ | ✔ | ✚ ✔ | ✚ | ✚ |  |  |  | ✚ ✚ | ✔ ✚ | ✔ | ✔ | ✔ |  | ✚ |
| Marine bilge discharge Marine plumbing Material chutes |  | ✔ | ✔ | ✚ | ✔ | ✔ |  | ✔ | ✚ ✚ | ✚ |  | ✚ | ✔ |  |  | ✔ |  |  |
| Material handling - heavy duty abrasive Material handling - standard duty Material handling - light duty |  | ✔ ✚ | ✔ ✚ | ✚ ✔ |  | ✚ |  |  |  | ✚ ✔ |  |  |  | ✔ | ✔ | ✔ |  |  |
| Milk and dairy product transfer Milling machine scrap recovery Mining applications (MSHA) | ✚ |  |  |  |  |  |  | ✚ |  | ✔ |  |  |  |  |  |  |  |  |
| Mulch, bark, wood chips, other surfacing materials Oil skimming Oil sluries |  | ✔ | ✔ |  |  |  |  |  |  | ✔ ✔ |  |  |  |  |  |  | ✚ ✚ |  |
| Oil suction Pharmaceutical product transfer Plastic processing equipment |  |  |  |  |  |  |  |  |  | ✚ |  |  |  |  |  |  | ✚ |  |
| Pneumatic conveying systems Poultry processing Pumps, rental and construction dewatering |  |  |  |  | ✚ | ✚ | ✚ | ✚ |  |  |  | ✚ | ✚ | ✚ | ✚ |  |  | ✚ |
| Pumps, trash Recreational vehicle (RV) pluming Rock dusting |  |  |  |  | ✚ | ✚ | ✚ ✔ | ✚ ✚ | ✚ |  |  | ✚ | ✚ | ✚ | ✚ ✚ | ✔ |  | ✚ |
| Rock, gravel, sand and crushed concrete vacuuming Septic and wastewater handling Sewer truck boom hose |  |  |  |  | ✔ | ✔ |  |  |  |  |  | ✚ | ✚ |  |  |  |  |  |
| Shot blast recovery Slurry handling Soil, seed and compost delivery |  |  | ✔ |  | ✔ | ✚ | ✔ |  |  |  |  |  | ✔ | ✚ |  | ✔ |  |  |
| Spa, pool and hot tub pluming Suction and discharge Wand hose |  |  | ✔ | ✔ |  |  |  |  |  |  | ✚ |  | ✚ |  |  |  |  | ✚ |
| Water suction - heavy duty Water suction - standard duty |  |  |  |  | ✔ ✚ | ✚ ✔ | ✚ ✔ | ✔ ✚ | ✔ | ✔ | ✔ | ✚ | ✚ ✔ | ✚ ✔ | ✚ ✔ | ✚ | ✔ | ✚ ✔ |

Application Guide

- Superior Product Design – Tigerflex™ WT™ series hoses are an industry standard for pneumatic material handling due to our specially engineered compound, innovative design and

uncompromising quality control. Provides the ideal combination of light weight, flexibility and durability.

- Food Grade Materials – Hose complies with applicable FDA(03) and 3-A(01) requirements. Hose approved by USDA(11) for use in meat and poultry plants.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Phthalate Free

WT™ Series

Food Grade PVC Material Handling Hose

General Applications:

- Food grade liquids such as potable water, beer, wine and juice

- Food grade material handling – standard duty

- Material handling – standard duty

- Pharmaceutical product transfer

- Plastic processing equipment

- Pneumatic conveying equipment

- Poultry processing

Construction: PVC tube with rigid PVC helix.

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

Features and Advantages:

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| WT100 | 1 | 25.4 | 1.30 | 33.0 | 55 | 30 | 28 | 28 | 2 | 100/50 | 0.21 |
| WT125 | 1-1/4 | 31.7 | 1.60 | 40.6 | 50 | 25 | 28 | 28 | 2 | 100/50 | 0.28 |
| WT150 | 1-1/2 | 38.1 | 1.92 | 48.8 | 50 | 25 | 28 | 28 | 3 | 100/50 | 0.35 |
| WT200 | 2 | 50.8 | 2.40 | 61.0 | 40 | 20 | 28 | 24 | 4 | 100/50 | 0.56 |
| WT225 | 2-1/4 | 57.2 | 2.74 | 69.6 | 40 | 20 | 28 | 24 | 4.5 | 100/50 | 0.65 |
| WT250 | 2-1/2 | 63.5 | 2.99 | 75.9 | 40 | 20 | 28 | 24 | 5 | 100/50 | 0.77 |
| WT300 | 3 | 76.2 | 3.64 | 92.5 | 40 | 20 | 28 | 24 | 6 | 100/50 | 1.10 |
| WT350 | 3-1/2 | 88.9 | 4.21 | 107.0 | 35 | 18 | 28 | 24 | 8 | 100/50 | 1.48 |
| WT400 | 4 | 101.6 | 4.72 | 120.0 | 35 | 18 | 24 | 22 | 10 | 100/50 | 1.80 |
| WT500 | 5 | 127.0 | 5.74 | 145.8 | 30 | 15 | 24 | 22 | 16 | 100/50/20 | 2.34 |
| WT600 | 6 | 152.4 | 6.91 | 175.5 | 30 | 15 | 24 | 22 | 18 | 100/50/20 | 3.70 |
| WT800 | 8 | 203.2 | 8.97 | 227.8 | 20 | 10 | 20 | 18 | 36 | 50/20 | 5.53 |
| WT45M | 1.77 | 45.0 | 2.09 | 53.0 | 45 | 25 | 28 | 24 | 4 | 100/50 | 0.44 |
| WT57M | 2.24 | 57.0 | 2.68 | 68.0 | 40 | 20 | 28 | 24 | 4.5 | 100/50 | 0.64 |
| WT60M | 2.36 | 60 | 2.8 | 71.1 | 40 | 20 | 28 | 24 | 4.5 | 100/50 | 0.71 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

3A(01), BSE/TSE(02) , FDA(03), Phthalate Free(09), RoHS(10), USDA(11)

  - Superior Product Design – Tigerflex™ WE™ series hoses are an industry standard for pneumatic material handling, due to our specially engineered compound, innovative design and

uncompromising quality control. Provides the ideal combination of light weight, flexibility and durability.

- Food Grade Materials – Hose complies with applicable FDA(03) requirements. Hose approved by USDA(11) for use in meat and poultry plants.

- Grounding Wire – Multi-strand wire helps prevent the build-up of static electricity for added safety and to help keep material flowing smoothly. It’s embedded within the rigid helix to prevent contamination of transferred materials.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Phthalate Free

WE™  Series

Food Grade PVC Material Handling Hose With Grounding Wire

General Applications:

- Food grade material handling – standard duty

- Material handling – standard duty

- Pharmaceutical product transfer

- Plastic processing equipment

- Pneumatic conveying equipment

Construction: PVC tube with rigid PVC helix and grounding wire.

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

Features and Advantages:

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| WE100 | 1 | 25.4 | 1.30 | 33.0 | 55 | 30 | 28 | 28 | 2 | 100/50 | 0.21 |
| WE125 | 1-1/4 | 32.0 | 1.65 | 42.0 | 50 | 25 | 28 | 28 | 2 | 100/60/50 | 0.33 |
| WE150 | 1-1/2 | 38.1 | 1.93 | 49.0 | 50 | 25 | 28 | 28 | 3 | 100/60/50 | 0.43 |
| WE200 | 2 | 50.8 | 2.48 | 63.0 | 40 | 20 | 28 | 24 | 4 | 100/60/50 | 0.58 |
| WE225 | 2-1/4 | 57.2 | 2.80 | 71.0 | 40 | 20 | 28 | 24 | 4.5 | 100/60/50 | 0.65 |
| WE250 | 2-1/2 | 63.5 | 3.07 | 76.5 | 40 | 20 | 28 | 24 | 5 | 100/60/50 | 0.89 |
| WE300 | 3 | 76.2 | 3.64 | 91.5 | 40 | 20 | 28 | 24 | 6 | 100/60/50 | 1.25 |
| WE350 | 3-1/2 | 88.9 | 4.27 | 108.5 | 35 | 18 | 28 | 24 | 8 | 100/60/50 | 1.55 |
| WE400 | 4 | 101.6 | 4.72 | 120.0 | 35 | 18 | 24 | 20 | 10 | 100/60/50 | 1.93 |
| WE500 | 5 | 127.0 | 5.74 | 146.0 | 30 | 15 | 24 | 20 | 16 | 60/50/20 | 2.40 |
| WE600 | 6 | 152.4 | 6.81 | 175.5 | 30 | 15 | 24 | 20 | 18 | 60/50/20 | 3.70 |
| WE800 | 8 | 204.8 | 9.06 | 230.0 | 20 | 10 | 20 | 18 | 36 | 20 | 5.62 |
| WE45M | 1.77 | 45.0 | 2.20 | 55.8 | 45 | 25 | 28 | 24 | 4 | 60 | 0.46 |
| WE57M | 2.24 | 57.0 | 2.76 | 70.0 | 40 | 20 | 28 | 24 | 4.5 | 60 | 0.64 |
| WE60M | 2.36 | 60.0 | 2.80 | 71.1 | 40 | 20 | 28 | 24 | 4.5 | 100/50 | 0.71 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

BSE/TSE(02), FDA(03), Phthalate Free(09), RoHS(10), USDA(11)

2001™  Series

Heavy Duty Food Grade Polyurethane Lined Material Handling Hose With Grounding Wire

### General Applications:

##### Food grade material handling

– heavy duty abrasive

  - Material handling – heavy duty abrasive

  - Pharmaceutical product transfer

  - Plastic processing equipment

  - Pneumatic conveying equipment

Construction: PVC cover with polyurethane liner, rigid PVC helix and grounding wire.

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

### Features and Advantages:

  - Extra Thick Abrasion Resistant Polyurethane Liner – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

  - Food Grade Materials – Hose cover complies with applicable FDA(03) requirements. Hose liner complies with applicable FDA(04) requirements. Hose approved by USDA(12) for use in meat and poultry plants.

- Phthalate Free

- Grounding Wire – Multi-strand wire helps prevent the build-up of static electricity for added safety and to help keep material flowing smoothly. It’s embedded within the rigid helix to prevent contamination of transferred materials.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Oil Resistant Polyurethane Liner – Resists most animal and petroleum based oils.

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| 2001–150 | 1-1/2 | 38.1 | 1.88 | 47.8 | 50 | 25 | Full | 28 | 6 | 60 | 0.48 |
| 2001–200 | 2 | 50.8 | 2.44 | 62.0 | 40 | 20 | Full | 28 | 7 | 60 | 0.67 |
| 2001–250 | 2-1/2 | 63.5 | 3.12 | 77.2 | 40 | 20 | Full | 28 | 8 | 60 | 0.92 |
| 2001–300 | 3 | 76.2 | 3.70 | 94.1 | 40 | 20 | Full | 28 | 9 | 60 | 1.35 |
| 2001–400 | 4 | 101.6 | 4.80 | 122.0 | 35 | 18 | Full | 28 | 15 | 60/20 | 2.17 |
| 2001–500 | 5 | 127.0 | 5.81 | 147.6 | 35 | 18 | 28 | 25 | 23 | 60/20 | 2.77 |
| 2001–600 | 6 | 152.4 | 6.93 | 176.0 | 30 | 15 | 28 | 25 | 26 | 60/20 | 3.90 |
| 2001–700 | 7 | 178.8 | 8.08 | 205.2 | 30 | 15 | 28 | 25 | 30 | 60/20 | 5.20 |
| 2001–800 | 8 | 203.2 | 9.28 | 235.8 | 30 | 15 | 28 | 25 | 36 | 20 | 6.65 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

### Features and Advantages:

  - Superior Static Protection! – A properly grounded Voltbuster™ hose will not retain an electrostatic charge sufficient to create a propagating brush discharge. Hose material, using the embedded grounding wire, shows a charge decay time constant of < 1 second, based on independent lab testing.

  - Food Grade Materials – Hose tube complies with FDA(05) requirements. Grounding wire embedded in external helix to prevent material contamination.

  - Extra Thick Abrasion Resistant Single-Ply Polyurethane Tube – Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

(+65°C)*

- Transparent Construction – “See-the-flow”. Allows for visual confirmation of material flow.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Easy Slide Helix – Rigid helix design protects hose tube from wear; allows hose to slide easily over rough surfaces. Easy to handle.

• Oil Resistant Polyurethane Tube – Resists most animal and petroleum based oils.

- Phthalate Free

VOLT™ Series

Heavy Duty Food Grade Static Dissipative Polyurethane

Material Handling Hose

General Applications:

- Bulk truck and railcar unloading

- Fly ash collection

- Food grade material handling – heavy duty abrasive

- Material handling – heavy duty abrasive

- Milling machine scrap recovery

- Pharmaceutical product transfer

- Plastic processing equipment

- Pneumatic conveying equipment

Construction: Static dissipative polyurethane tube, rigid helix and grounding wire (patent pending).

Service Temperature: -40°F (-40°C) to 150°F

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| VOLT150 | 1-1/2 | 38.35 | 1.87 | 47.5 | 40 | 20 | Full | 28 | 2 | 100/60 | 0.31 |
| VOLT200 | 2 | 51.1 | 2.52 | 63.9 | 40 | 20 | Full | 28 | 6 | 100/60 | 0.61 |
| VOLT250 | 2-1/2 | 63.75 | 2.96 | 75.2 | 40 | 20 | Full | 28 | 7 | 100/50 | 0.76 |
| VOLT300 | 3 | 76.2 | 3.60 | 91.4 | 40 | 20 | Full | 28 | 9 | 100/60 | 0.91 |
| VOLT400 | 4 | 101.6 | 4.69 | 121.0 | 35 | 17 | 28 | 25 | 12 | 100/60/20 | 1.70 |
| VOLT500 | 5 | 127.0 | 5.75 | 146.8 | 35 | 17 | 28 | 25 | 14 | 60/20 | 2.13 |
| VOLT600 | 6 | 153.4 | 6.81 | 173.2 | 30 | 15 | 25 | 20 | 16 | 60/20 | 2.53 |
| VOLT800 | 8 | 203.5 | 8.76 | 223.3 | 30 | 15 | 25 | 20 | 18 | 20 | 3.30 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

BSE/TSE(02), FDA(05), Phthalate Free(09),RoHS(10)

BBeeccaauussee wwee ccoonnttiinnuuaallllyy eexxaammiinnee wwaayyss ttoo iimmpprroovvee oouurr pprroodduuccttss,, wwee rreesseerrvvee tthhee rriigghhtt ttoo aalltteerr ssppeecciifificcaattiioonnss oorr ddiissccoonnttiinnuuee pprroodduuccttss wwiitthhoouutt pprriioorr nnoottiiccee..

### Features and Advantages:

  - Extra Thick Abrasion Resistant Double-Ply Polyurethane Tube – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

  - Food Grade Materials – Hose liner complies with applicable FDA(04) requirements. Hose approved by USDA(12) for use in meat and poultry plants.

  - Fabric Reinforcement – Designed with high tensile strength, food grade(05), polyester yarn jacket to handle both suction, and higher pressure discharge applications.

  - Grounding Wire – Multi-strand wire helps prevent the build-up of static electricity for added safety and to help keep material flowing smoothly. It’s embedded within the rigid helix to prevent contamination of transferred materials.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to- handle.

- Oil Resistant Polyurethane Tube – Resists most animal and petroleum based oils.

- Phthalate Free

2020™ Series

Heavy Duty Food Grade Polyurethane Fabric Reinforced Material Handling Hose With Grounding Wire

General Applications:

- Bulk truck and railcar unloading

- Food grade material handling – heavy duty abrasive

- Material handling – heavy duty abrasive

- Suction and discharge

Construction: Extra thick double-ply polyurethane tube, polyester fabric reinforcement, rigid PVC helix and grounding wire.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| 2020-200 | 2 | 50.1 | 2.65 | 67.5 | 75 | 40 | Full | 28 | 9 | 100 | 0.94 |
| 2020-300 | 3 | 76.2 | 3.78 | 96.0 | 70 | 35 | Full | 28 | 10 | 100/50/20 | 1.20 |
| 2020-400 | 4 | 101.6 | 4.84 | 123.0 | 65 | 30 | Full | 28 | 12 | 100/50/20 | 1.60 |
| 2020-500 | 5 | 127.0 | 5.79 | 147.0 | 45 | 22 | 28 | 25 | 14 | 50/25/20 | 2.45 |
| 2020-600 | 6 | 152.4 | 6.93 | 176.0 | 40 | 22 | 28 | 25 | 16 | 50/25/20 | 2.86 |
| 2020-800 | 8 | 206.0 | 9.21 | 234.0 | 30 | 15 | 24 | 20 | 22 | 50/20 | 4.69 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

# VLT-SD™ Series

## Heavy Duty Food Grade Static Dissipative Polyurethane

Fabric Reinforced Material Handling Hose

### Features and Advantages:

  - Superior Static Protection! – A properly grounded Voltbuster™ hose will not retain an electrostatic charge sufficient to create a propagating brush discharge. Hose material, using the embedded grounding wire, shows a charge decay time constant of < 1 second, based on independent lab testing.

  - Food Grade Materials – Hose tube complies with FDA(05) requirements. Grounding wire embedded in external helix to prevent material contamination.

  - Extra Thick Abrasion Resistant Double-Ply Polyurethane Tube – Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

- Phthalate Free

General Applications:

- Bulk truck and railcar unloading

- Food grade material handling – heavy duty abrasive

- Material handling – heavy duty abrasive

- Milling machine scrap recovery

- Plastic processing equipment

- Pneumatic conveying equipment

- Suction and discharge

Construction: Static dissipative polyurethane tube, polyester fabric reinforcement, rigid helix and grounding wire (patent pending).

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

- Fabric Reinforcement – Designed with high tensile strength, food grade FDA(06), polyester yarn jacket to handle both suction, and higher pressure discharge applications.

- Transparent Construction – “See-the-flow”. Allows for visual conformation of material flow.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Easy Slide Helix – Rigid helix design protects hose

from wear; allows hose to slide easily over rough surfaces. Easy to handle.

- Oil Resistant Polyurethane Tube – Resists most animal and petroleum based oils.

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| VLT-SD200 | 2 | 51.1 | 2.67 | 67.0 | 75 | 40 | Full | 28 | 9 | 100/50 | 0.77 |
| VLT-SD300 | 3 | 77.0 | 3.78 | 96.0 | 70 | 35 | Full | 28 | 12 | 100/20 | 1.22 |
| VLT-SD400 | 4 | 102.2 | 4.84 | 123.0 | 65 | 30 | Full | 28 | 13 | 100/60/20 | 1.85 |
| VLT-SD500 | 5 | 128.0 | 5.79 | 152.0 | 45 | 22 | 28 | 25 | 14 | 60/20 | 2.43 |
| VLT-SD600 | 6 | 153.4 | 6.93 | 177.4 | 40 | 22 | 28 | 25 | 17 | 60/20 | 3.05 |
| VLT-SD800 | 8 | 206.0 | 9.25 | 235.0 | 35 | 25 | 26 | 20 | 23 | 20 | 4.70 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

BSE/TSE(02), FDA(05), FDA(06), Phthalate Free(09), RoHS(10)

# WBS™ Series

## Food Grade PVC Material Handling Hose

### With Static Dissipative Additives

General Applications:

##### Food grade material handling – standard duty

  - Material handling – standard duty

  - Pharmaceutical product transfer

  - Plastic processing equipment

  - Pneumatic conveying equipment

Construction: Static dissipative PVC tube with rigid PVC helix.

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

### Features and Advantages:

  - Abrasion Resistant PVC Tube – Formulated from highly durable PVC compounds for increased abrasion resistance.

  - Food Grade Materials – Hose complies with applicable FDA(03) requirements. Hose approved by USDA(11) for use in meat and poultry plants.

  - Static Dissipative Tube – Specially formulated to help

prevent the build-up of static electricity for added safety and to help keep material flowing smoothly.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| WBS150 | 1-1/2 | 38.1 | 1.92 | 48.8 | 50 | 25 | 28 | 28 | 3 | 100 | 0.35 |
| WBS200 | 2 | 50.8 | 2.40 | 61.0 | 40 | 20 | 28 | 24 | 4 | 100 | 0.56 |
| WBS250 | 2-1/2 | 63.5 | 2.99 | 75.9 | 40 | 20 | 28 | 24 | 5 | 100 | 0.77 |
| WBS300 | 3 | 76.2 | 3.64 | 92.5 | 40 | 20 | 28 | 24 | 6 | 100 | 1.10 |
| WBS400 | 4 | 101.6 | 4.76 | 121.0 | 35 | 20 | 24 | 20 | 10 | 100/50 | 1.92 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: The effectiveness of static dissipation is application-dependent, based upon humidity, material conveyed, and length of hose.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

BSE/TSE(02), FDA(03), Phthalate Free(09), RoHS(10), USDA(11)

### Features and Advantages:

  - Food Grade Materials – Hose complies with applicable FDA(03) and 3-A(01) requirements. Hose approved by USDA(12) for use in meat and poultry plants.

  - Fabric Reinforcement – Designed with high tensile strength, food grade, FDA(06) polyester yarn jacket to handle both suction, and higher pressure discharge applications.

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Phthalate Free

WSTF™ Series

Food Grade PVC Fabric Reinforced

Suction & Discharge Hose

eneral Applications:

- Food grade liquids such as potable water, beer, wine and juice

- Food grade material handling – standard duty

- Ice transfer

- Suction and discharge

- Water suction – heavy duty

Construction: Double-ply PVC tube, polyester fabric reinforcement and rigid PVC helix.

G

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| WSTF150 | 1-1/2 | 38.1 | 1.95 | 49.5 | 110 | 70 | Full | 28 | 2.5 | 100 | 0.42 |
| WSTF200 | 2 | 50.8 | 2.60 | 66.0 | 100 | 65 | Full | 28 | 4 | 100 | 0.74 |
| WSTF300 | 3 | 76.2 | 3.62 | 92.0 | 100 | 50 | Full | 28 | 6 | 100/20 | 1.13 |
| WSTF400 | 4 | 101.6 | 4.76 | 121.0 | 75 | 37 | Full | 28 | 8 | 100/20 | 1.74 |
| WSTF600 | 6 | 152.4 | 7.17 | 182.1 | 70 | 35 | 28 | 25 | 13 | 100/20 | 3.88 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

3A(01), BSE/TSE(02), FDA(03), FDA(06), Phthalate Free(09), RoHS(10), USDA(11)

# MILK™ Series

## Food Grade

PVC Liquid Suction Hose

MILK-LT™ Series

Low Temperature Food Grade

PVC Liquid Suction Hose

### General Applications:

MILK

MILK-LT

(low temp)

  - Food grade liquids such as potable water, beer, wine and juice

  - Ice transfer

  - Milk and dairy product transfer

  - Water suction – standard duty

Construction: PVC tube with rigid PVC helix. Service Temperature (MILK): -4°F (-20°C) to 150°F (+65°C)*

Service Temperature (MILK-LT): -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

  - Precision Controlled ID and OD Dimensions – Facilitates insertion of sanitary fittings.

  - Food Grade Materials – Hose complies with applicable FDA(03) and 3-A(01) requirements. Hose approved by USDA(11) for use in meat and poultry plants.

  - “Cold-Flex” Materials (MILK-LT only) – Hose remains flexible in severe sub-zero temperatures.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Smooth Outer Cover – Provides increased pressure rating and smooth surface for banding.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| MILK150 | 1-1/2 | 38.1 | 1.79 | 45.5 | 75 | 50 | Full | 26 | 4 | 100 | 0.45 |
| MILK200 | 2 | 50.8 | 2.33 | 59.2 | 75 | 50 | 28 | 25 | 6 | 100 | 0.63 |
| MILK250 | 2-1/2 | 63.5 | 2.87 | 73.0 | 55 | 40 | 28 | 24 | 10 | 100 | 0.81 |
| MILK300 | 3 | 76.2 | 3.42 | 86.9 | 55 | 40 | 28 | 24 | 11 | 100 | 1.18 |
| MILK-LT150 | 1-1/2 | 38.1 | 1.79 | 45.5 | 75 | 50 | Full | 26 | 4 | 100 | 0.45 |
| MILK-LT200 | 2 | 50.8 | 2.33 | 59.2 | 75 | 50 | 28 | 25 | 5 | 100 | 0.65 |
| MILK-LT250 | 2-1/2 | 63.5 | 2.87 | 73.0 | 55 | 40 | 28 | 24 | 8 | 100 | 0.84 |
| MILK-LT300 | 3 | 76.2 | 3.42 | 86.9 | 55 | 40 | 28 | 24 | 11 | 100 | 1.20 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

Features and Advantages:

  - Food Grade Materials – Hose complies with applicable FDA(03) and 3-A(01) requirements. Hose approved by USDA(11) for use in meat and poultry plants.

  - Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Smooth Outer Cover – Provides increased pressure rating and smooth surface for banding.

- Phthalate Free

FT™  Series

Heavy Duty Food Grade PVC Suction Hose

General Applications:

- Food grade liquids such as potable water, beer, wine and juice

- Food grade material handling – standard duty

- Ice transfer

- Milk and dairy product transfer

- Poultry processing

- Water suction – heavy duty

Construction: PVC tube with rigid PVC helix. Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| FT075 | 3/4 | 19.0 | 0.94 | 24.0 | 115 | 75 | Full | 28 | 3 | 100 | 0.17 |
| FT100 | 1 | 25.5 | 1.28 | 32.5 | 100 | 70 | Full | 28 | 3 | 100 | 0.24 |
| FT125 | 1-1/4 | 32.0 | 1.56 | 39.6 | 90 | 65 | Full | 28 | 4 | 100 | 0.44 |
| FT150 | 1-1/2 | 38.1 | 1.80 | 46.5 | 85 | 60 | Full | 28 | 6 | 100 | 0.50 |
| FT200 | 2 | 50.8 | 2.36 | 60.0 | 85 | 60 | Full | 26 | 8 | 100 | 0.71 |
| FT250 | 2-1/2 | 63.5 | 2.88 | 73.2 | 65 | 45 | Full | 26 | 10 | 100 | 0.94 |
| FT300 | 3 | 76.2 | 3.42 | 86.9 | 55 | 40 | Full | 24 | 11 | 100 | 1.14 |
| FT400 | 4 | 101.6 | 4.51 | 114.6 | 50 | 35 | Full | 24 | 18 | 100/60 | 1.91 |
| FT500 | 5 | 127.0 | 5.51 | 140.0 | 40 | 25 | 28 | 23 | 28 | 100/20 | 2.41 |
| FT600 | 6 | 153.4 | 6.59 | 167.4 | 30 | 20 | 28 | 15 | 48 | 20 | 3.28 |
| FT800 | 8 | 204.7 | 8.85 | 224.7 | 25 | 15 | 28 | 10 | 60 | 20 | 5.67 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

3A(01), BSE/TSE(02), FDA(03), Phthalate Free(09), RoHS(10), USDA(11)

# GTF™ Series

## Food Grade PVC Ducting/Material Handling Hose

GTFE™ Series

Food Grade PVC Ducting/Material Handling Hose

with Grounding Wire

### General Applications:

##### Ducting, ventilation and fume removal

  - Food grade blower and ducting systems

  - Material handling – light duty

  - Pharmaceutical product transfer

GTF

ed e)

GTFE

(with embedd grounding wir

Construction: PVC tube with rigid PVC helix and grounding wire (GTFE Series).

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

### Features and Advantages:

  - Food Grade Materials – Hose complies with applicable FDA(03) and 3-A(01) requirements. Hose approved by USDA(11) (GTF only) for use in meat and poultry plants.

  - Grounding Wire (GTFE only) – Multi-strand wire helps prevent the build-up of static electricity for added safety and to help keep material flowing smoothly. It’s embedded within the rigid helix to prevent contamination of transferred materials.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Easy Slide Helix – Exposed rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| GTF/GTFE150 | 1-1/2 | 38.1 | 1.82 | 46.2 | 20 | 7 | 22 | 14 | 1 | 100 | 0.23 |
| GTF/GTFE200 | 2 | 50.8 | 2.39 | 60.8 | 15 | 6 | 21 | 12 | 2 | 100 | 0.30 |
| GTF/GTFE250 | 2-1/2 | 63.5 | 2.89 | 73.4 | 10 | 5 | 19 | 10 | 2 | 100 | 0.39 |
| GTF/GTFE300 | 3 | 76.2 | 3.46 | 87.9 | 10 | 5 | 18 | 10 | 3 | 100/50 | 0.50 |
| GTF/GTFE400 | 4 | 101.6 | 4.50 | 114.3 | 8 | 4 | 13 | 7 | 3 | 100/50 | 0.77 |
| GTF/GTFE600 | 6 | 152.4 | 6.54 | 166.1 | 6 | 3 | 7 | 5 | 6 | 50 | 1.08 |
| GTF/GTFE800 | 8 | 203.2 | 8.59 | 218.2 | 4 | 2 | 5 | 3 | 8 | 50 | 1.74 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed. Not for liquid handling use.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

# UVF™ Series

## Food Grade Polyurethane Ducting/ Material Handling Hose

### General Applications:

##### Ducting, ventilation and fume removal

  - Dust collection

  - Food grade blower and ducting systems

  - Food grade material handling – standard duty

  - Pharmaceutical product transfer Construction: Polyurethane tube with rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

- Durable Lightweight Polyurethane Tube – Designed for dry applications where abrasion is a factor. Provides longer hose life and lower operating costs versus rubber or PVC hoses.

- Food Grade Materials – Hose complies with applicable FDA(04) requirements. Hose approved by USDA(12) for use in meat and poultry plants.

- Transparent Construction – “See-the-flow”. Allows for visual confirmation of material flow.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Easy Slide Helix – Exposed rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Oil Resistant Polyurethane Hose – Resists most animal and petroleum based oils.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| UVF150 | 1-1/2 | 38.1 | 1.82 | 46.2 | 20 | 7 | 22 | 14 | 1 | 50 | 0.23 |
| UVF200 | 2 | 50.8 | 2.39 | 60.7 | 15 | 6 | 21 | 12 | 1.5 | 50 | 0.32 |
| UVF250 | 2-1/2 | 63.5 | 2.89 | 73.4 | 10 | 5 | 19 | 10 | 1.5 | 50 | 0.39 |
| UVF300 | 3 | 76.2 | 3.46 | 87.9 | 10 | 5 | 18 | 10 | 2.5 | 50 | 0.55 |
| UVF400 | 4 | 101.6 | 4.50 | 114.3 | 8 | 4 | 13 | 8 | 3 | 50 | 0.77 |
| UVF500 | 5 | 127.0 | 5.50 | 139.7 | 7 | 3 | 10 | 7 | 4 | 50 | 0.89 |
| UVF600 | 6 | 152.4 | 6.54 | 166.1 | 6 | 3 | 7 | 5 | 5 | 50 | 1.15 |
| UVF800 | 8 | 203.2 | 8.59 | 218.1 | 4 | 2 | 5 | 3 | 7 | 50/20 | 1.75 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

BSE/TSE(02), FDA(04), Phthalate Free(09), RoHS(10), USDA(11)

### Features and Advantages:

  - Superior Rubber Compounds – Tigerflex™ uses specially engineered compounds which provide the ideal combina- tion of excellent abrasion resistance, light weight, flexibility, static dissipation and superior long-lasting durability.

  - Static Dissipative Tube – Specially formulated to help prevent the build-up of static electricity for added safety and to help keep material flowing smoothly.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Phthalate Free

Tiger™ TR1™ Series

Heavy Duty SBR Wet or Dry Material Handling Hose

General Applications:

- Fly ash collection

- Grain Handling

- Hydro excavation

- Industrial vacuum equipment

- Material handling – heavy duty abrasive

- Milling machine scrap recovery

- Rock, gravel, sand and crushed concrete vacuuming

- Sewer truck boom hose

- Shot blast recovery

- Slurry handling

Construction: SBR rubber tube with rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| TR1-150 | 1-1/2 | 38.5 | 1.94 | 49.2 | 35 | 26 | Full | 28 | 1.5 | 100 | 0.50 |
| TR1-200 | 2 | 50.8 | 2.38 | 60.5 | 32 | 23 | Full | 26 | 1.5 | 100/50 | 0.70 |
| TR1-250 | 2-1/2 | 63.4 | 3.05 | 77.5 | 30 | 22 | Full | 26 | 2.0 | 100/50 | 0.84 |
| TR1-300 | 3 | 76.2 | 3.56 | 90.5 | 28 | 20 | Full | 26 | 2.5 | 100/50 | 1.00 |
| TR1-400 | 4 | 101.6 | 4.67 | 118.5 | 26 | 18 | Full | 26 | 4.5 | 100/50 | 1.70 |
| TR1-500 | 5 | 126.8 | 5.73 | 145.5 | 21 | 16 | 28 | 24 | 5.0 | 100/50 | 2.38 |
| TR1-600 | 6 | 153.4 | 7.03 | 178.8 | 19 | 13 | 28 | 24 | 9.5 | 100/50/20 | 5.13 |
| TR1-800 | 8 | 204.8 | 9.27 | 255.6 | 19 | 13 | 27 | 23 | 14 | 50/20 | 7.34 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

*Actual service temperature range is application dependent.

Available with grounding wire upon request. Minimum order required, contact Kuriyama customer service for details.

Service Temperature: -40°F (-40°C) to 220°F (+104°C)*

### Features and Advantages:

  - Wire Reinforced Helix – Highly durable steel helical wire provides strength and allows for use at higher temperatures without risk of hose deformation. Wire can be grounded for additional static dissipation.

  - Static Dissipative Tube - Specially formulated to help prevent the build-up of static electricity for added safety and to help keep material flowing smoothly.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Convoluted Cover Design – Provides increased hose flexibility.

- Phthalate Free

Rated up to 220°F!

Tiger™ “HiTemp” THT™ Series

Wire Reinforced EPDM Wet or Dry Material Handling Hose

General Applications:

- Agricultural liquid fertilizer

- Fly ash collection

- Hydroexcavation

- Industrial vacuum equipment

- Material chutes

- Milling machine scrap recovery

- Rock, gravel, sand and crushed concrete vacuuming

- Sewer truck boom hose

- Slurry handling

Construction: EPDM tube and polyethylene helix with steel helical wire.

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in. @ 68°F) | Standard Lengths (ft.) | Weight (lbs./ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| THT400 | 4 | 101.6 | 4.63 | 117.6 | 29 | 21 | Full | 26 | 5.5 | 100/20 | 1.90 |
| THT600 | 6 | 152.4 | 6.87 | 178.4 | 19 | 14 | 27 | 24 | 10.0 | 100/50/20 | 3.65 |
| THT800 | 8 | 204.8 | 9.06 | 229.8 | 14 | 10 | 27 | 24 | 15.0 | 50/20 | 5.94 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

Amphibian™ AMPH™  Series

## Heavy Duty Polyurethane

Lined Wet or Dry Material Handling Hose

### General Applications:

##### Agricultural dry fertilizers

  - Air seeder lines

  - Fly ash collection

  - Hydro excavation

  - Industrial vacuum equipment

  - Material handling – heavy duty abrasive

  - Milling machine scrap recovery

  - Rock, gravel, sand and crushed concrete vacuuming

  - Sewer truck boom hose

  - Shot blast recovery

  - Slurry handling

Construction: PVC cover with polyurethane liner and rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

  - Thick Amphibian™ Abrasion Resistant Polyurethane Liner – Designed for wet or dry applications where severe abrasion is a factor. Provides longer hose life and lower operating costs versus rubber or PVC hoses.

  - Static Dissipative Cover – Specially formulated to help prevent the build-up of static electricity for added safety and to help keep material flowing smoothly.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Convoluted Cover Design – Provides increased hose flexibility.

- Oil Resistant Polyurethane Liner – Resists most animal and petroleum based oils.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| AMPH400 | 4 | 101.6 | 4.76 | 120.9 | 35 | 18 | Full | 28 | 8 | 100 | 1.95 |
| AMPH500 | 5 | 127.0 | 5.75 | 146.0 | 36 | 18 | 28 | 25 | 15 | 100/20 | 2.42 |
| AMPH600 | 6 | 152.4 | 6.81 | 173.0 | 30 | 15 | 28 | 25 | 18 | 100/20 | 3.50 |
| AMPH800 | 8 | 203.2 | 9.18 | 233.2 | 30 | 15 | 28 | 25 | 22 | 60/21 | 5.91 |

Features and Advantages:

  - Extra Thick Abrasion Resistant Polyurethane Liner – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

  - Static Dissipative Cover – Specially formulated to help prevent the build-up of static electricity for added safety and to help keep material flowing smoothly.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Oil Resistant Polyurethane Liner – Resists most animal and petroleum based oils.

- Phthalate Free

Ureflex™ UF2™ Series

Extra Heavy Duty

Polyurethane Lined Material Handling Hose

General Applications:

- Fly ash collection

- Industrial vacuum equipment

- Material chutes

- Material handling – heavy duty abrasive

- Milling machine scrap recovery

- Rock, gravel, sand and crushed concrete vacuuming

- Shot blast recovery

Construction: PVC cover with polyurethane liner and rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| UF2-150 | 1-1/2 | 38.1 | 1.88 | 47.8 | 50 | 25 | Full | 28 | 3 | 100 | 0.46 |
| UF2-200 | 2 | 50.8 | 2.44 | 62.0 | 40 | 20 | Full | 28 | 4 | 100 | 0.65 |
| UF2-250 | 2-1/2 | 63.5 | 3.12 | 79.2 | 40 | 20 | Full | 28 | 5 | 100 | 0.89 |
| UF2-300 | 3 | 76.2 | 3.70 | 94.1 | 40 | 20 | Full | 28 | 6 | 100/50 | 1.23 |
| UF2-400 | 4 | 101.6 | 4.80 | 122.0 | 35 | 18 | Full | 28 | 10 | 100/50 | 2.02 |
| UF2-500 | 5 | 127.0 | 5.81 | 147.6 | 35 | 18 | 28 | 25 | 15 | 100/50/20 | 2.50 |
| UF2-600 | 6 | 152.4 | 6.87 | 174.5 | 30 | 15 | 28 | 25 | 18 | 100/50/20 | 3.84 |
| UF2-800 | 8 | 203.2 | 9.18 | 233.2 | 30 | 15 | 28 | 25 | 22 | 50/20 | 6.52 |
| UF2-1000 | 10 | 254.0 | 11.61 | 295.0 | 25 | 12 | 26 | 20 | 26 | 20 | 10.92 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

Ureflex™ UF1™ Series

Heavy Duty Polyurethane

Lined Material Handling Hose

General Applications:

  - Agricultural dry fertilizers

  - Air seeder lines

  - Fly ash collection

  - Industrial vacuum equipment

  - Material chutes

  - Material handling – heavy duty abrasive

  - Milling machine scrap recovery

  - Rock, gravel, sand and crushed concrete vacuuming

  - Shot blast recovery

Construction: PVC cover with polyurethane liner and rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

  - Thick Abrasion Resistant Polyurethane Liner – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

  - Static Dissipative Cover – Specially formulated to help prevent the build-up of static electricity for added safety and to help keep material flowing smoothly.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Oil Resistant Polyurethane Liner – Resists most animal and petroleum based oils.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| UF1-125 | 1-1/4 | 31.8 | 1.53 | 39.0 | 50 | 25 | Full | 28 | 2 | 100 | 0.22 |
| UF1-150 | 1-1/2 | 38.1 | 1.85 | 47.0 | 50 | 25 | Full | 28 | 2 | 100/50 | 0.42 |
| UF1-200 | 2 | 50.8 | 2.40 | 61.0 | 40 | 20 | Full | 28 | 3 | 100/50 | 0.59 |
| UF1-250 | 2-1/2 | 63.5 | 3.07 | 78.0 | 40 | 20 | Full | 28 | 3 | 100/50 | 0.80 |
| UF1-300 | 3 | 76.2 | 3.64 | 92.5 | 40 | 20 | Full | 28 | 4 | 100/50 | 1.18 |
| UF1-350 | 3-1/2 | 88.9 | 4.21 | 107.0 | 35 | 18 | Full | 28 | 5 | 100/50 | 1.48 |
| UF1-400 | 4 | 101.6 | 4.76 | 120.9 | 35 | 18 | Full | 28 | 6 | 100/50 | 1.95 |
| UF1-500 | 5 | 127.0 | 5.75 | 146.0 | 35 | 18 | 28 | 25 | 10 | 100/50/20 | 2.42 |
| UF1-600 | 6 | 152.4 | 6.81 | 173.0 | 30 | 15 | 28 | 25 | 12 | 100/50/20 | 3.50 |
| UF1-800 | 8 | 203.2 | 9.18 | 233.2 | 30 | 15 | 28 | 25 | 18 | 50/20 | 5.91 |
| UF1-1000 | 10 | 255.0 | 11.60 | 294.5 | 22 | 10 | 24 | 18 | 26 | 20 | 9.90 |

UBK™ Series

Heavy Duty Polyurethane Lined Material Handling Hose

General Applications:

  - Agricultural dry fertilizers

  - Air seeder lines

  - Fly ash collection

  - Industrial vacuum equipment

  - Material handling – heavy duty abrasive

  - Milling machine scrap recovery

  - Rock, gravel, sand and crushed concrete vacuuming

  - Shot blast recovery

Construction: PVC cover with polyurethane liner and rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

- Thick Abrasion Resistant Polyurethane Liner – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

- Static Dissipative Cover – Specially formulated to help prevent the build-up of static electricity for added safety and to help keep material flowing smoothly.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Oil Resistant Polyurethane Liner – Resists most animal and petroleum based oils.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| UBK200 | 2 | 50.8 | 2.40 | 61.0 | 40 | 15 | Full | 28 | 2 | 100/50 | 0.59 |
| UBK250 | 2-1/2 | 63.5 | 3.07 | 78.0 | 40 | 15 | Full | 28 | 4 | 100/50 | 0.79 |
| UBK300 | 3 | 76.2 | 3.64 | 92.5 | 40 | 15 | Full | 28 | 4 | 100/50 | 0.83 |
| UBK400 | 4 | 101.6 | 4.76 | 120.9 | 35 | 13 | Full | 28 | 6 | 100/50 | 1.37 |
| UBK500 | 5 | 127.0 | 5.69 | 144.5 | 30 | 10 | 28 | 15 | 10 | 100/50/20 | 2.28 |
| UBK600 | 6 | 152.4 | 6.81 | 173.0 | 30 | 10 | 28 | 15 | 12 | 100/50/20 | 3.10 |
| UBK800 | 8 | 203.2 | 9.02 | 229.0 | 30 | 10 | 28 | 15 | 15 | 50/20 | 4.51 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

Ureflex™ UFC™ Series

Heavy Duty Polyurethane

Lined Material Handling Hose

General Applications:

  - Agricultural dry fertilizer

  - Air seeder lines

  - Industrial vacuum equipment

  - Material handling – heavy duty abrasive

  - Milling machine scrap recovery

  - Plastic processing equipment

  - Shot blast recovery

Construction: PVC cover with polyurethane liner and rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

  - Thick Abrasion Resistant Polyurethane Liner – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

  - Static Dissipative Cover – Specially formulated to help prevent the build-up of static electricity for added safety and to help keep material flowing smoothly.

- Phthalate Free

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Oil Resistant Polyurethane Liner – Resists most animal and petroleum based oils.

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| UFC150 | 1-1/2 | 38.1 | 1.85 | 47.0 | 50 | 25 | Full | 28 | 2 | 100 | 0.42 |
| UFC200 | 2 | 50.8 | 2.40 | 61.0 | 40 | 20 | Full | 28 | 3 | 100 | 0.59 |
| UFC250 | 2-1/2 | 63.5 | 3.07 | 78.0 | 40 | 20 | Full | 28 | 3 | 100 | 0.80 |
| UFC300 | 3 | 76.2 | 3.64 | 92.5 | 40 | 20 | Full | 28 | 4 | 100 | 1.18 |
| UFC400 | 4 | 101.6 | 4.76 | 120.9 | 35 | 18 | Full | 28 | 6 | 100 | 1.95 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

Features and Advantages:

  - Extra Thick Single-Ply Abrasion Resistant Polyurethane Tube – Our thickest single-ply polyurethane tube! Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

  - Grounding Wire – Multi-strand wire helps prevent the

build-up of static electricity for added safety and to help keep material flowing smoothly. It’s embedded within the rigid helix to prevent contamination of transferred materials.

  - Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Oil Resistant Polyurethane Tube – Resists most animal and petroleum based oils.

- Phthalate Free

G

Plas-T-Flo™ PF™ Series

Heavy Duty Food Grade Polyurethane Material Handling Hose

With Grounding Wire

eneral Applications:

- Bulk truck & railcar unloading

- Material handling – heavy duty abrasive

- Milling machine scrap recovery

- Plastic processing equipment

Construction: Polyurethane tube with rigid PVC helix and grounding wire.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| PF300 | 3 | 76.2 | 3.39 | 86.0 | 35 | 15 | 28 | 25 | 10 | 100/20 | 1.50 |
| PF400 | 4 | 101.6 | 4.84 | 123.0 | 30 | 15 | 28 | 25 | 12 | 100/50/20 | 1.96 |
| PF500 | 5 | 127.0 | 5.87 | 149.0 | 30 | 15 | 25 | 22 | 13 | 100/50/20 | 2.50 |
| PF600 | 6 | 152.4 | 6.91 | 175.5 | 30 | 15 | 25 | 22 | 16 | 100/50/20 | 3.18 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

BSe/tSe(02), FDA(03), FDA(04), Phthalate Free(09), RoHS(10), USDA(11)

Urevac™ UV3™ Series

## Heavy Duty Polyurethane

Material Handling Hose With Grounding Wire

### General Applications:

##### Dust collection

  - Material handling – heavy duty abrasive

  - Milling machine scrap recovery

  - Plastic processing equipment

  - Trench suction

Construction: Single-ply polyurethane tube with rigid PVC helix and grounding wire.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

  - Thick Abrasion Resistant Single-Ply Polyurethane Tube – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

  - Grounding Wire – Multi-strand wire helps prevent the

build-up of static electricity for added safety and to help keep material flowing smoothly. It’s embedded within the rigid helix to prevent contamination of transferred materials.

- Phthalate Free

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Oil Resistant Polyurethane Tube – Resists most animal and petroleum based oils.

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| UV3-300 | 3 | 76.2 | 3.60 | 91.4 | 40 | 20 | Full | 28 | 9 | 100/50 | 0.91 |
| UV3-400 | 4 | 101.6 | 4.66 | 118.4 | 35 | 17 | 28 | 25 | 12 | 100/50 | 1.50 |
| UV3-500 | 5 | 127.0 | 5.50 | 145.0 | 35 | 17 | 28 | 25 | 14 | 50/20 | 1.82 |
| UV3-600 | 6 | 152.4 | 6.65 | 172.0 | 30 | 15 | 25 | 20 | 16 | 50/20 | 2.24 |
| UV3-800 | 8 | 203.5 | 8.76 | 223.0 | 30 | 15 | 25 | 20 | 18 | 50/20 | 3.00 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

### Features and Advantages:

  - Abrasion Resistant Polyurethane Liner – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus similar rubber or PVC hoses.

  - “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

  - Static Dissipative Cover – Specially formulated to help prevent the build-up of static electricity for added safety and to help keep material flowing smoothly.

Urevac™ UV2™ Series

## Heavy Duty Polyurethane

Lined Ducting/Material Handling Hose

### General Applications:

##### Agricultural dry fertilizer

- Air seeder lines

- Dust control

- Material handling – standard duty

- Wand hose

Construction: PVC cover with ester polyurethane (TPU) liner and rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Oil Resistant Polyurethane Liner – Resists most animal and petroleum based oils.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID |  | OD |  | Working Pressure (PSI) |  | Vacuum Rating (in Hg) |  | Min. Bending Radius (in.) @ 68°F | Standard Length (ft.) | Weight (lbs/ ft) |
|  | (in.) | (mm) | (in.) | (mm) | 68°F | 104°F | 68°F | 104°F |  |  |  |
| UV2-150 | 1-1/2 | 38.1 | 1.87 | 47.5 | 25 | 10 | 22 | 16 | 1.5 | 60 | 0.29 |
| UV2-200 | 2 | 50.8 | 2.47 | 62.7 | 25 | 10 | 21 | 14 | 2.5 | 60 | 0.40 |
| UV2-250 | 2-1/2 | 63.5 | 2.96 | 75.2 | 20 | 8 | 19 | 12 | 3 | 60 | 0.53 |
| UV2-300 | 3 | 76.2 | 3.54 | 89.8 | 20 | 8 | 18 | 11 | 4 | 60 | 0.67 |
| UV2-400 | 4 | 101.6 | 4.57 | 116.1 | 15 | 7 | 13 | 9 | 6 | 60 | 1.02 |
| UV2-500 | 5 | 127.0 | 5.58 | 141.7 | 15 | 7 | 10 | 7 | 8 | 60 | 1.22 |
| UV2-600 | 6 | 152.4 | 6.62 | 168.1 | 10 | 5 | 7 | 5 | 10 | 60 | 1.68 |
| UV2-800 | 8 | 203.2 | 8.67 | 220.2 | 10 | 5 | 5 | 3 | 14 | 20 | 2.24 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

  - Thick Abrasion Resistant Polyurethane Tube – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

  - Crush Resistant Construction – Hose rebounds to shape without structural damage when crushed; material keeps flowing.

  - Grounding Wire – Multi-strand wire helps prevent the

build-up of static electricity for added safety and to help keep material flowing smoothly.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Oil Resistant Polyurethane Tube – Resists most animal and petroleum based oils.

- Phthalate Free

UVPE™  Series

Heavy Duty Polyurethane Material Handling Hose With Grounding Wire

General Applications:

- Material handling – heavy duty abrasive

- Plastic processing equipment Construction: Polyurethane tube with rigid polypropylene helix.

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| UVPE150 | 1-1/2 | 38.1 | 1.87 | 47.5 | 20 | 7 | 22 | 14 | 3 | 100 | 0.39 |
| UVPE200 | 2 | 50.8 | 2.44 | 62.0 | 15 | 6 | 21 | 12 | 4 | 100 | 0.48 |
| UVPE250 | 2-1/2 | 63.5 | 2.99 | 75.9 | 10 | 5 | 19 | 10 | 5 | 100 | 0.55 |
| UVPE300 | 3 | 76.2 | 3.64 | 92.5 | 10 | 5 | 18 | 10 | 6 | 100 | 0.68 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

# “Ground Cover” GC-C™ Series

## Heavy Duty Polyurethane Lined Material Handling Hose

### Features and Advantages:

  - Abrasion Resistant Polyurethane Liner – Designed for dry applications where severe abrasion is a factor. Provides longer hose life and lower operating costs versus rubber or PVC hoses.

  - “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Phthalate Free

General Applications:

- Material handling – heavy duty abrasive

- Mulch, bark, wood chips and other surfacing material delivery

- Soil, seed and compost delivery

Construction: PVC cover with Polyurethane liner and rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Convoluted Outer Cover – Provides increased hose flexibility. Allows for easier unwinding and winding on hose reels.

- Oil Resistant Polyurethane Liner – Resists most animal and petroleum based oils.

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| GC-C400 | 4 | 101.6 | 4.59 | 116.6 | 30 | 15 | 28 | 25 | 6 | 100 | 1.00 |
| GC-C500 | 5 | 127.0 | 5.57 | 141.5 | 30 | 15 | 25 | 20 | 10 | 100 | 1.80 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

“Mulch Hose” MULCH™ Series

Heavy Duty PVC

Material Handling Hose

MULCH-LT™ Series

Heavy Duty PVC Low Temperature

Material Handling Hose

General Applications:

  - Material handling – standard duty

  - Mulch, bark, wood chips and other surfacing material delivery

  - Soil, seed and compost delivery

Construction: PVC tube and rigid PVC helix. Service Temperature (MULCH): -4°F (-20°C) to 150°F (+65°C)*

Service Temperature (MULCH-LT): -40°F (-40°C) to 150°F (+65°C)*

MUL

CH

MULCH-LT

(low temp)

Features and Advantages:

  - Abrasion Resistant PVC Tube – Formulated from highly durable PVC compounds for increased abrasion and tear resistance versus standard PVC hoses.

  - “Cold-Flex” Materials (MULCH-LT only) – Hose remains flexible in sub-zero temperatures.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| MULCH400 | 4 | 101.6 | 4.57 | 116.0 | 35 | 15 | Full | 28 | 8 | 100 | 1.42 |
| MULCH500 | 5 | 127.0 | 5.61 | 142.6 | 30 | 12 | 24 | 22 | 14 | 100 | 1.75 |
| MULCH600 | 6 | 153.4 | 6.79 | 172.4 | 25 | 10 | 24 | 22 | 16 | 100 | 2.42 |
| MULCH-LT400 | 4 | 101.6 | 4.57 | 116.0 | 35 | 15 | Full | 28 | 8 | 100 | 1.35 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

Features and Advantages:

  - Abrasion Resistant PVC Tube – Formulated from highly durable PVC compounds for increased abrasion and tear resistance versus standard PVC hoses.

  - Convoluted Outer Cover – Provides increased hose flexibility. Allows for easier unwinding and winding on hose reels.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Phthalate Free

“Bark Hose”

BARK™  Series

Standard Duty PVC Material Handling Hose

General Applications:

- Lawn and leaf collection

- Material handling – standard duty

- Mulch, bark, wood chips and other surfacing material delivery

- Soil, seed and compost delivery

Construction: PVC tube with rigid PVC helix. Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| BARK400 | 4 | 101.6 | 4.45 | 113 | 18 | 11 | 15 | 10 | 10 | 100 | 0.95 |
| BARK500 | 5 | 127.0 | 5.47 | 139 | 17 | 10 | 14 | 8 | 11 | 100 | 1.29 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

Features and Advantages:

  - “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

  - Transparent Construction (LKC series only) – “See-the- flow.” Allows for visual confirmation of material flow.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Phthalate Free

Lawn King™

LK™ Series LKC™  Series

PVC Ducting/Material Handling Hose

General Applications:

- Dust collection

- Lawn and leaf collection

- Material handling – light duty

Construction: PVC tube with rigid PVC helix.

Service Temperature: -20°F (-29°C) to 150°F (+65°C)*

LK

LKC

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| LK/LKC400 | 4 | 101.6 | 4.57 | 114.8 | 8 | 4 | 13 | 7 | 3 | 100/50 | 0.85 |
| LKC500 | 5 | 128.0 | 5.55 | 141.0 | 7 | 3 | 10 | 6 | 5 | 100 | 0.93 |
| LK600 | 6 | 152.4 | 6.63 | 168.3 | 6 | 3 | 7 | 5 | 6 | 50 | 1.34 |
| LKC600 | 6 | 152.4 | 6.63 | 168.3 | 6 | 3 | 7 | 5 | 6 | 100/50 | 1.34 |
| LKC700 | 7 | 177.8 | 7.56 | 192.0 | 4 | 2 | 6 | 4 | 7 | 50 | 1.53 |
| LK/LKC800 | 8 | 203.2 | 8.63 | 219.3 | 4 | 2 | 5 | 3 | 8 | 50 | 2.00 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

NEW

### Features and Advantages:

UV1

UVE

Urevac™ UV1™  Series

## Polyurethane Ducting/

Material Handling Hose

UVE™ Series

Polyurethane Ducting/ Material Handling Hose With Grounding Wire

### General Applications:

- Concrete resurfacing dust collection

- Ducting, ventilation and fume removal

- Dust collection

- Insulation blowing

- Material chutes

- Material handling – standard duty

Construction: Ester polyurethane (TPU) tube with rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

  - Durable Lightweight Polyurethane Tube – Designed for dry applications where abrasion is a factor. Provides longer hose life and lower operating costs versus rubber or PVC hoses.

  - Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

  - Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

  - “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Oil Resistant Polyurethane Tube – Resists most animal and petroleum based oils.

- Grounding Wire (UVE only) – Multi-strand wire helps prevent the build-up of static electricity for added safety and to help keep material flowing smoothly. It’s embedded within the rigid helix to prevent contamination of transferred materials.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID |  | OD |  | Working Pressure (PSI) |  | Vacuum Rating (in. Hg) |  | Min. Bending Radius (in.) @ 68°F | Standard Length (ft.) |  | Weight (lbs/ ft) |
|  | (in.) | (mm) | (in.) | (mm) | 68°F | 104°F | 68°F | 104°F |  | UV1 50 | UVE 100/50 |  |
| UV1-150 | 1 1/2 | 38.1 | 1.82 | 46.2 | 20 | 7 | 22 | 14 | 0.75 | 50 |  | 0.23 |
| UV1/UVE-200 | 2 | 50.8 | 2.39 | 60.7 | 15 | 6 | 21 | 12 | 1.5 | 100/50 |  | 0.32 |
| UV1-250 | 2 1/2 | 63.5 | 2.89 | 73.4 | 10 | 5 | 19 | 10 | 1.5 | 50 |  | 0.39 |
| UV1/UVE-300 | 3 | 76.2 | 3.46 | 87.9 | 10 | 5 | 18 | 10 | 2.5 | 100/50 |  | 0.58 |
| UV1/UVE-400 | 4 | 101.6 | 4.50 | 114.3 | 8 | 4 | 13 | 8 | 3 | 100/50 |  | 0.77 |
| UV1-500 | 5 | 127.0 | 5.50 | 139.7 | 7 | 3 | 10 | 7 | 4 | 50 |  | 0.89 |
| UV1/UVE-600 | 6 | 152.4 | 6.54 | 166.1 | 6 | 3 | 7 | 5 | 5 | 100/50 |  | 1.15 |
| UV1-800 | 8 | 203.2 | 8.59 | 218.2 | 4 | 2 | 5 | 3 | 7 | 50 |  | 1.75 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

GTG now Anti-Microbial!

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

### Features and Advantages:

  - Transparent Construction (GT series only) – “See-the- flow.” Allows for visual confirmation of material flow.

  - Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Anti-Microbial Tube (GTG series only) – Inhibits growth of bacteria, fungi, mold and yeast.

- Phthalate Free

GT™ Series GTG™ Series

PVC Ducting/Material Handling Hose

General Applications:

- Cable protection

- Drain lines

- Ducting, ventilation and fume removal

- Dust collection

- Material handling – light duty

Construction: PVC tube with rigid PVC helix.

GT

G

GT

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| GT/GTG150 | 1-1/2 | 38.1 | 1.82 | 46.2 | 20 | 7 | 22 | 14 | 1 | 100/50 | 0.23 |
| GT/GTG200 | 2 | 50.8 | 2.39 | 60.8 | 15 | 6 | 21 | 12 | 2 | 100/50 | 0.30 |
| GT238 | 2-3/8 | 60.3 | 2.76 | 70.1 | 12 | 6 | 10 | 5 | 2 | 100 | 0.38 |
| GT/GTG250 | 2-1/2 | 63.5 | 2.89 | 73.4 | 10 | 5 | 19 | 10 | 2 | 100/50 | 0.39 |
| GT/GTG300 | 3 | 76.2 | 3.46 | 87.9 | 10 | 5 | 18 | 10 | 3 | 100/50 | 0.50 |
| GT350 | 3-1/2 | 88.9 | 4.02 | 102.0 | 9 | 4 | 15 | 8 | 3 | 100/50 | 0.68 |
| GT/GTG400 | 4 | 101.6 | 4.50 | 114.3 | 8 | 4 | 13 | 7 | 3 | 100/50 | 0.77 |
| GT500 | 5 | 127.0 | 5.50 | 139.7 | 7 | 3 | 10 | 6 | 5 | 100/50 | 0.91 |
| GT600 | 6 | 152.4 | 6.54 | 166.1 | 6 | 3 | 7 | 5 | 6 | 100/50 | 1.08 |
| GT800 | 8 | 203.2 | 8.59 | 218.2 | 4 | 2 | 5 | 3 | 8 | 50 | 1.74 |
| GT1000 | 10 | 254.0 | 11.68 | 296.6 | 2 | — | 2 | — | 10 | 50 | 2.70 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

Features and Advantages:

  - MSHA(08) Approved – Meets U.S. Dept. of Labor Administration requirements for flame-resistance for use in mines for protection of hose bundles. Optional, special order, red or green colored helix also approved.

  - Transparent Construction – “See-the-flow.” Allows for visual confiurmation of material flow.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- CG-SL Series – pre-slit for easy insertion of hose bundles.

- Phthalate Free

“Cover Guard”

CG™/CG-SL™ Series

PVC Ducting and Cover Protection Hose

General Applications:

- Cable and hose bundle protection (MSHA)

- Dust collection

- Ducting, ventilation and fume removal

- Mine supply line cover protection

Construction: PVC tube with rigid PVC helix.

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

CG-SL

(pre-slit)

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| CG-SL100 | 1 | 25.4 | 1.28 | 31.9 | n/a | n/a | n/a | n/a | .5 | 100 | 0.14 |
| CG-SL125 | 1-1/4 | 31.8 | 1.51 | 38.4 | n/a | n/a | n/a | n/a | .75 | 100 | 0.18 |
| CG-SL150 | 1-1/2 | 38.1 | 1.76 | 45.1 | n/a | n/a | n/a | n/a | 1 | 100 | 0.21 |
| CG/CG-SL200 | 2 | 50.8 | 2.30 | 58.4 | 12 | 6 | 10 | 5 | 2 | 100 | 0.28 |
| CG238 | 2-3/8 | 60.3 | 2.76 | 70.1 | 12 | 6 | 10 | 5 | 2 | 100 | 0.38 |
| CG/CG-SL250 | 2-1/2 | 63.5 | 2.81 | 71.3 | 10 | 5 | 8 | 4 | 2 | 100 | 0.39 |
| CG/CG-SL300 | 3 | 76.2 | 3.35 | 85.0 | 8 | 4 | 7 | 3 | 3 | 100 | 0.45 |
| CG/CG-SL350 | 3-1/2 | 88.9 | 3.83 | 97.4 | 8 | 4 | 7 | 3 | 3 | 100 | 0.51 |
| CG/CG-SL400 | 4 | 102.4 | 4.39 | 111.4 | 6 | 3 | 6 | 3 | 3 | 100 | 0.64 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

MSHA(08), Phthalate Free(09), RoHS(10)

### Features and Advantages:

  - Transparent Construction (H & K Series only) – “See-the- flow.” Allows for visual confirmation of material flow.

  - MSHA(07) Approved (J Series only) – Approved by the Mine Safety and Health Administration for flame-resistance for use in underground mines as water transfer hose.

- Smooth Outer Cover (Sizes 3/4” – 5”) – Provides increased pressure rating and smooth surface for banding.

- Convoluted Outer Cover (Sizes 6” & 8”) – Provides increased hose flexibility.

- Phthalate Free

H™/J™/K™ Series

Standard Duty PVC Suction Hose

H

J

General Applications:

- Agricultural liquid fertilizer

- Air seeder lines

- Drain lines

- Irrigation lines

- Mining applications

- Pumps, rental and construction dewatering

- Pumps, trash

- Rock dusting

- Water suction – standard duty

Construction: PVC tube with rigid PVC helix. Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

K

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| H/J/K075 | 3/4 | 19.0 | 1.01 | 25.6 | 110 | 70 | 28 | 26 | 3 | 100 | 0.19 |
| H/J/K100 | 1 | 25.4 | 1.26 | 32.0 | 85 | 60 | 28 | 26 | 3 | 100 | 0.26 |
| H/J/K125 | 1-1/4 | 31.7 | 1.56 | 39.6 | 85 | 60 | 28 | 24 | 4 | 100 | 0.35 |
| H/J/K150 | 1-1/2 | 38.1 | 1.83 | 46.5 | 70 | 50 | 28 | 24 | 5 | 100 | 0.48 |
| H/J/K200 | 2 | 50.8 | 2.32 | 59.0 | 65 | 45 | 28 | 24 | 7 | 100 | 0.66 |
| H/J/K250 | 2-1/2 | 63.5 | 2.87 | 73.0 | 65 | 45 | 28 | 24 | 8 | 100 | 0.87 |
| H/J/K300 | 3 | 76.2 | 3.43 | 87.0 | 60 | 40 | 28 | 22 | 10 | 100 | 1.24 |
| H/J/K400 | 4 | 101.6 | 4.50 | 114.7 | 50 | 35 | 28 | 22 | 15 | 100 | 1.85 |
| H500 | 5 | 127.0 | 5.58 | 141.3 | 45 | 30 | 28 | 24 | 22 | 100/20 | 2.42 |
| H/J/K600 | 6 | 152.4 | 6.75 | 171.4 | 40 | 25 | 28 | 20 | 30 | 100/20 | 3.39 |
| H/J/K800 | 8 | 203.2 | 8.86 | 225.0 | 30 | 20 | 26 | 20 | 35 | 20 | 5.63 |

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

MSHA(07), Phthalate Free(09), RoHS(10)

### Features and Advantages:

  - Transparent Construction (F Series only) – “See-the-flow.” Allows for visual confirmation of material flow.

  - “Safety Orange” Color (G Series Only) – For high visibility on job site. Reduces risk of running or tripping over hose.

- Smooth Outer Cover (Sizes 3/4” – 5”) – Provides increased pressure rating and smooth surface for banding.

- Convoluted Outer Cover (Sizes 6” & 8”) – Provides increased hose flexibility.

- Phthalate Free

F

G

S

Tiger™ Suction F™/G™/S™ Series

Heavy Duty PVC

Suction Hose

General Applications:

- Irrigation lines

- Pumps, rental and construction dewatering

- Pumps, trash

- Water suction – heavy duty

Construction: PVC tube with rigid PVC helix. Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| F075 | 3/4 | 19.0 | 1.01 | 25.6 | 115 | 75 | Full | 28 | 3 | 100 | 0.21 |
| F/G/S100 | 1 | 25.4 | 1.26 | 32.0 | 100 | 65 | Full | 28 | 3 | 100 | 0.27 |
| F/S125 | 1-1/4 | 31.7 | 1.56 | 39.6 | 100 | 65 | Full | 26 | 4 | 100 | 0.36 |
| F/G/S150 | 1-1/2 | 38.1 | 1.83 | 46.5 | 100 | 65 | Full | 26 | 5 | 100 | 0.48 |
| F/G/S200 | 2 | 50.8 | 2.38 | 60.4 | 100 | 65 | Full | 26 | 7 | 100 | 0.71 |
| F/G250 | 2-1/2 | 63.5 | 2.89 | 73.4 | 70 | 48 | Full | 26 | 8 | 100 | 0.96 |
| F/G/S300 | 3 | 76.2 | 3.44 | 87.4 | 70 | 45 | Full | 26 | 10 | 100 | 1.25 |
| F/G/S400 | 4 | 101.6 | 4.57 | 116.1 | 60 | 40 | Full | 26 | 15 | 100 | 1.95 |
| F500 | 5 | 127.0 | 5.59 | 141.9 | 45 | 30 | 28 | 24 | 22 | 100/20 | 2.45 |
| F/G600 | 6 | 152.4 | 6.77 | 172.0 | 40 | 25 | 28 | 22 | 25 | 100/20 | 3.76 |
| F/G800 | 8 | 203.2 | 8.90 | 226.1 | 30 | 20 | 28 | 18 | 30 | 20 | 6.00 |

“Blue Water” BW™ Series

Low Temperature PVC Suction Hose

General Applications:

  - Extreme cold conditions

  - Pumps, rental and construction dewatering

  - Pumps, trash

  - Water suction – standard duty

Construction: PVC tube with rigid PVC helix. Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

  - “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures. Beware of imitations! Blue Water™ truly remains flexible in extreme cold.

  - Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Smooth Outer Cover (Sizes 1” - 4”) – Provides increased pressure rating and smooth surface for banding.

- Convoluted Outer Cover (Sizes 5” & 6”) – Provides increased hose flexibility.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| BW075 | 3/4 | 19.1 | 1.01 | 25.6 | 115 | 75 | Full | 28 | 3 | 100 | 0.19 |
| BW100 | 1 | 25.4 | 1.26 | 32.0 | 90 | 65 | Full | 28 | 3 | 100 | 0.22 |
| BW125 | 1-1/4 | 31.8 | 1.56 | 39.6 | 90 | 65 | Full | 26 | 4 | 100 | 0.36 |
| BW150 | 1-1/2 | 38.1 | 1.79 | 45.5 | 90 | 65 | Full | 26 | 5 | 100 | 0.48 |
| BW200 | 2 | 50.8 | 2.35 | 59.8 | 90 | 65 | Full | 26 | 7 | 100 | 0.62 |
| BW250 | 2-1/2 | 63.5 | 2.87 | 73.0 | 70 | 48 | Full | 26 | 8 | 100 | 0.87 |
| BW300 | 3 | 76.2 | 3.43 | 87.0 | 65 | 45 | Full | 26 | 10 | 100 | 1.23 |
| BW400 | 4 | 101.6 | 4.49 | 114.0 | 55 | 40 | Full | 26 | 15 | 100 | 1.83 |
| BW500 | 5 | 127.0 | 5.57 | 141.5 | 45 | 30 | 28 | 24 | 25 | 100/20 | 2.42 |
| BW600 | 6 | 152.4 | 6.69 | 170.0 | 40 | 25 | 28 | 22 | 30 | 100/20 | 3.36 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

NOTE: Refer to Storage and Handling, and Max Coil Stack Height on page 65.

*Actual service temperature range is application dependent.

Cold Flex™ CF™  Series

## Extra Heavy Duty Low Temperature PVC Suction Hose

### General Applications:

##### Extreme cold conditions

  - Irrigation lines

  - Material handling – standard duty

  - Pumps, rental and construction dewatering

  - Pumps, trash

  - Slurry handling

  - Water suction – heavy duty

Construction: PVC tube with rigid PVC helix. Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

### Features and Advantages:

- Superior Vacuum Rating – Our toughest and most durable liquid suction hose! Extremely thick hose tube and extra large helix provide for a tough, durable hose with all sizes rated to full vacuum (at 68°F).

- Cold Flex™ Materials – Hose remains flexible in severe sub-zero temperatures.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Static Dissipative Tube – Specially formulated to help prevent the build-up of static electricity for added safety and help keep material flowing smoothly.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| CF150 | 1-1/2 | 38.1 | 1.84 | 46.7 | 100 | 65 | Full | 28 | 3 | 100 | 0.40 |
| CF200 | 2 | 50.8 | 2.41 | 61.2 | 100 | 65 | Full | 28 | 4 | 100 | 0.75 |
| CF250 | 2-1/2 | 63.5 | 2.93 | 74.5 | 90 | 55 | Full | 28 | 6 | 100 | 0.99 |
| CF300 | 3 | 76.2 | 3.59 | 91.2 | 80 | 50 | Full | 28 | 7 | 100 | 1.34 |
| CF400 | 4 | 101.6 | 4.67 | 118.6 | 65 | 35 | Full | 28 | 11 | 100 | 2.15 |
| CF600 | 6 | 152.4 | 6.87 | 174.4 | 50 | 25 | Full | 28 | 18 | 100/50/20 | 3.76 |
| CF800† | 8 | 204.75 | 9.13 | 232.0 | 35 | 15 | Full | 26 | 24 | 20 | 6.59 |

W™  Series

## Heavy Duty PVC Liquid Suction Hose

### General Applications:

##### Extreme cold conditions (Sizes 4" - 16")

  - Fish suction

  - Gold dredging

  - Pumps, rental and construction dewatering

  - Pumps, trash

  - Slurry handling

  - Water suction – heavy duty

Construction: PVC tube with rigid PVC helix.

### Service Temperature:

##### Sizes 1" - 3": -4°F (-20°C) to 150°F (+65°C)*; Sizes 4" - 16": -40°F (-40°C) to 150°F (+65°C)*

Features and Advantages:

  - “Cold-Flex” Materials (Sizes 4" - 16") – Hose remains flexible in sub-zero temperatures.

  - Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Convoluted Outer Cover – Provides increased hose flexibility.

The Original Heavy Duty Suction

Hose

Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| W100 | 1 | 25.4 | 1.30 | 33.0 | 55 | 35 | Full | 28 | 1 | 100 | 0.21 |
| W125 | 1-1/4 | 31.7 | 1.60 | 40.6 | 50 | 30 | Full | 28 | 2 | 100 | 0.28 |
| W150 | 1-1/2 | 38.1 | 1.85 | 47.0 | 50 | 30 | Full | 28 | 2 | 100 | 0.34 |
| W200 | 2 | 50.8 | 2.40 | 61.0 | 50 | 30 | Full | 28 | 3 | 100 | 0.52 |
| W250 | 2-1/2 | 63.5 | 2.99 | 75.9 | 45 | 25 | Full | 28 | 4 | 100 | 0.77 |
| W300 | 3 | 76.2 | 3.64 | 92.5 | 45 | 25 | Full | 28 | 6 | 100 | 1.18 |
| W400 | 4 | 101.6 | 4.76 | 121.0 | 35 | 18 | Full | 28 | 8 | 100 | 1.92 |
| W500 | 5 | 127.0 | 5.75 | 146.0 | 35 | 18 | 28 | 25 | 12 | 100/20 | 2.42 |
| W600 | 6 | 152.4 | 7.00 | 177.8 | 30 | 15 | 28 | 25 | 14 | 100/20 | 3.76 |
| W800 | 8 | 203.2 | 9.18 | 233.2 | 30 | 15 | 28 | 25 | 24 | 40/20 | 5.99 |
| W1000 | 10 | 254.0 | 11.56 | 293.5 | 25 | 12 | 28 | 25 | 39 | 40/20 | 9.74 |
| W1200 | 12 | 304.8 | 13.64 | 346.5 | 20 | 10 | 28 | 25 | 59 | 40/20 | 12.77 |
| W1400† | 14 | 357.6 | 15.59 | 396.0 | 18 | 8 | 26 | 23 | 80 | 20 | 13.50 |
| W1600† | 16 | 408.4 | 17.72 | 450.0 | 12 | 5 | 24 | 20 | 95 | 20 | 16.00 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

†Non-stock item, minimum order required. Contact Kuriyama customer service for details.

Our Most Flexible Suction Hose

### Features and Advantages:

  - “Cold-Flex” Materials (SH Series; Sizes 2½" - 8") –

Hose remains flexible in sub-zero temperatures.

  - Transparent Construction – “See-the-flow.” Allows for visual conformation of material flow.

- Drain lines

- Dust collection

- Gold dredging

- Water suction – standard duty

Construction: PVC tube with rigid PVC helix. Service Temperature (WH Series): -4ºF (-20ºC) to 150ºF (+65ºC)*

Service Temperature (SH Series): -40ºF (-40ºC) to 150ºF (+65ºC)*

- Convoluted Outer Cover – Provides increased hose flexibility.

- Phthalate Free

WH™  Series

Standard Duty PVC Liquid Suction Hose

SH™  Series

Standard Duty Low Temperature

PVC Liquid Suction Hose

General Applications:

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| WH100 | 1 | 25.4 | 1.22 | 31.0 | 45 | 15 | Full | 24 | 1 | 100 | 0.15 |
| WH125 | 1-1/4 | 31.8 | 1.54 | 39.2 | 40 | 12 | Full | 24 | 1 | 100 | 0.20 |
| WH150 | 1-1/2 | 38.1 | 1.80 | 45.7 | 40 | 12 | Full | 24 | 1.5 | 100 | 0.25 |
| WH200 | 2 | 50.8 | 2.32 | 58.7 | 35 | 10 | 26 | 20 | 2.5 | 100 | 0.31 |
| SH250 | 2-1/2 | 63.5 | 9.97 | 75.5 | 30 | 9 | 24 | 18 | 3 | 100 | 0.43 |
| SH300 | 3 | 76.2 | 3.48 | 88.4 | 25 | 7 | 24 | 18 | 4 | 100 | 0.64 |
| SH400 | 4 | 101.6 | 5.52 | 114.8 | 25 | 7 | 18 | 14 | 6 | 100 | 1.06 |
| SH500 | 5 | 127.0 | 5.57 | 141.5 | 20 | 6 | 16 | 12 | 10 | 100 | 1.47 |
| SH600 | 6 | 153.4 | 6.69 | 169.9 | 20 | 6 | 14 | 10 | 12 | 100 | 2.27 |
| SH800 | 8 | 204.8 | 8.86 | 225.0 | 10 | 3 | 12 | 8 | 24 | 60 | 3.34 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

WST™ Series

Heavy Duty PVC Fabric Reinforced Suction & Discharge Hose

General Applications:

  - Fish suction

  - Irrigation lines

  - Pumps, rental and construction dewatering

  - Pumps, trash

  - Suction and discharge

  - Water suction – heavy duty

Construction: Double-ply PVC tube, polyester fabric reinforcement and rigid PVC helix.

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

### Features and Advantages:

  - Fabric Reinforcement – Designed with high tensile strength polyester yarn jacket to handle both suction and higher pressure discharge applications.

  - Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces. Easy-to-handle.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| WST150 | 1-1/2 | 38.1 | 1.95 | 49.5 | 110 | 70 | Full | 28 | 2.5 | 100 | 0.42 |
| WST200 | 2 | 50.8 | 2.60 | 66.0 | 100 | 65 | Full | 28 | 4 | 100 | 0.74 |
| WST300 | 3 | 76.2 | 3.62 | 92.0 | 100 | 50 | Full | 28 | 6 | 100/20 | 1.13 |
| WST400 | 4 | 101.6 | 4.76 | 121.0 | 75 | 37 | Full | 28 | 8 | 100/20 | 1.74 |
| WST500 | 5 | 127.0 | 5.98 | 151.9 | 70 | 35 | 28 | 25 | 11 | 100/20 | 2.95 |
| WST600 | 6 | 152.4 | 7.17 | 182.1 | 70 | 35 | 28 | 25 | 13 | 100/20 | 3.88 |
| WST800 | 8 | 203.5 | 9.21 | 234.0 | 60 | 30 | 26 | 20 | 18 | 25/20 | 5.57 |

Features and Advantages:

  - Highly Durable PVC Tube – Formulated from highly durable PVC compound for increased abrasion and tear resistance.

  - Convoluted Outer Cover – Provides increased hose flexibility.

- Phthalate Free

Construction: PVC tube with rigid PVC helix. Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

WG™ Series

Heavy Duty PVC Liquid Suction Hose

General Applications:

- Fish suction

- Irrigation lines

- Pumps, rental and construction dewatering

- Pumps, trash

- Rock dusting

- Water suction – heavy duty

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| WG150 | 1-1/2 | 38.1 | 1.85 | 47.0 | 50 | 25 | Full | 28 | 2 | 100 | 0.34 |
| WG200 | 2 | 50.8 | 2.40 | 61.0 | 50 | 25 | Full | 28 | 3 | 100 | 0.52 |
| WG300 | 3 | 76.2 | 3.64 | 92.5 | 45 | 25 | Full | 28 | 6 | 100 | 1.18 |
| WG400 | 4 | 101.6 | 4.76 | 120.9 | 35 | 18 | Full | 28 | 8 | 100 | 1.93 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

“Marine Hose” MH™ Series

PVC Suction Hose

General Applications:

- Drain lines

- Marine bilge discharge

- Marine plumbing

- Recreational vehicle (RV) plumbing

Construction: PVC tube with rigid PVC helix. Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

### Features and Advantages:

- Odor-resistant Tube – Special additives help eliminate the build-up of unwanted odors.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Easy Installation – Ideal for working in confined areas. Permits installers to make smooth, tight turns. Requires fewer fittings than rigid pipe.

- Phthalate Free

Part No. A2150L1

Custom Molded Cuff — 11/2" Molded cuff (shown above) is designed for use with Tigerflex® Series MH150 marine hose.

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| MH100 | 1 | 25.4 | 1.22 | 31.0 | 45 | 15 | Full | 24 | 1 | 100 | 0.15 |
| MH125 | 1-1/4 | 32.0 | 1.49 | 38.0 | 40 | 12 | Full | 24 | 1.5 | 100 | 0.20 |
| MH150 | 1-1/2 | 38.1 | 1.77 | 45.0 | 40 | 12 | Full | 24 | 2 | 100 | 0.25 |
| MH200 | 2 | 50.8 | 2.32 | 59.0 | 35 | 10 | 26 | 20 | 2.5 | 100 | 0.31 |

# “Spa Hose” FMCR™ Series

## PVC Suction Hose

### General Applications:

##### Commonly referred to as “flex pipe”

  - Drain lines

  - Spa, pool and hot tub plumbing

Construction: PVC tube with rigid PVC helix.

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

### Features and Advantages:

- Precision Controlled OD – Designed to be glued into Schedule 40 PVC fittings.

- Easy Installation – Ideal for working in confined areas. Permits installers to make smooth, tight turns. Requires fewer fittings than rigid pipe when plumbing a normal spa or hot tub application.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | IPS Size (in.) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| F16MCR | 1/2 | 0.850 | 21.50 | 100 | 70 | 28 | 26 | 2 | 100/50 | 0.14 |
| F20MCR | 3/4 | 1.053 | 26.75 | 100 | 70 | 28 | 26 | 2 | 100/50 | 0.21 |
| F27MCR | 1 | 1.320 | 33.52 | 100 | 70 | 28 | 24 | 3 | 100/50 | 0.28 |
| F36MCR | 1-1/4 | 1.663 | 42.25 | 80 | 55 | 28 | 24 | 4 | 100/50 | 0.37 |
| F42MCR | 1-1/2 | 1.904 | 48.35 | 70 | 50 | 28 | 24 | 4 | 100/50 | 0.44 |
| F52MCR | 2 | 2.381 | 60.48 | 70 | 50 | 28 | 24 | 6 | 100/50 | 0.58 |
| F78MCR | 3 | 3.500 | 89.00 | 65 | 40 | 28 | 22 | 8 | 50 | 1.20 |

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

NOTE: Use with recommended primers and PVC cements; consult with glue supplier for recommendations. Coils of Tigerflex® Spa Hose should not be stacked more than five coils high. Hose which has been stacked high may be damaged over time.

NOTE: Black color available upon request. Minimum order quantity may apply. Contact Kuriyama customer service for details.

*Actual service temperature range is application dependent.

Product Warning

Like other materials, Spa Hoses can be damaged by rodents or insects, including termites. Our warranty does not cover damages caused by them. Spa Hose should not be used underground in areas infested by termites. This product warning shall be given to every purchaser of Spa Hose. (Rev. 7/98)

### Features and Advantages:

  - Superior Rubber Compounds – Tigerflex™ uses only the best available EPDM compounds, which provide the ideal combination of light-weight, flexibility, durability and chemical resistance.

  - Superior Flexibility – Our tests show up to 22% more flexible than the competition, especially in sub-zero weather! Tiger™ Green comes off the trucks more flexible and easier to handle than other similar hoses.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces and around corners. Easy-to-handle.

- Convoluted Outer Cover – Provides increased hose flexibility.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Phthalate Free

Tiger™ Green TG™ Series

EPDM Suction Hose

General Applications:

- Agriculture liquid fertilizers

- Irrigation lines

- Liquid manure handling

- Marine bilge discharge

- Pumps, rental and construction dewatering

- Pumps, trash

- Septic and wastewater handling

- Used frack solution removal

- Water suction – standard duty

Construction: EPDM tube with polyethylene helix. Service Temperature: -40°F (-40°C) to 160°F (+71°C)*

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| TG100 | 1 | 25.4 | 1.40 | 35.5 | 65 | 45 | FULL | 28 | 2 | 100 | 0.28 |
| TG125 | 1-1/4 | 31.8 | 1.63 | 41.4 | 60 | 40 | FULL | 28 | 3 | 100 | 0.33 |
| TG150 | 1-1/2 | 38.1 | 1.93 | 49.0 | 50 | 35 | FULL | 28 | 3 | 100 | 0.44 |
| TG200 | 2 | 50.8 | 2.51 | 63.8 | 50 | 35 | FULL | 28 | 5 | 100 | 0.67 |
| TG250 | 2-1/2 | 63.5 | 3.07 | 78.0 | 45 | 30 | FULL | 28 | 5.5 | 100 | 0.95 |
| TG300 | 3 | 76.2 | 3.60 | 91.5 | 45 | 30 | FULL | 26 | 7 | 100 | 1.14 |
| TG400 | 4 | 101.6 | 4.70 | 119.5 | 40 | 25 | FULL | 26 | 11.5 | 100 | 1.84 |
| TG600 | 6 | 152.4 | 6.85 | 174.0 | 30 | 20 | 28 | 24 | 20 | 100/20 | 3.07 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

NOTE: Other colors available upon request. Minimum order quantity may apply. Contact Kuriyama Tigerflex department for details.

Service Temperature: -40°F (-40°C) to 160°F (+71°C)*

### Features and Advantages:

  - Superior Rubber Compounds – Tigerflex™ uses only the best available EPDM compounds, which provide the ideal combination of light-weight, flexibility, durability and chemical resistance.

  - Superior Flexibility – Our tests show up to 22% more flexible than the competition, especially in sub-zero weather! Tiger™ Green comes off the trucks more flexible and easier to handle than other similar hoses.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces and around corners. Easy-to-handle.

- Convoluted Outer Cover – Provides increased hose flexibility.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Phthalate Free

G

•

•

Tiger™ Yellow

TY™  Series

EPDM Suction Hose

eneral Applications:

Agriculture liquid fertilizers Irrigation lines

- Liquid manure handling

- Marine bilge discharge

- Pumps, rental and construction dewatering

- Pumps, trash

- Septic and wastewater handling

- Used frack solution removal

- Water suction – standard duty

Construction: EPDM tube with polyethylene helix.

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| TY100 | 1 | 25.4 | 1.40 | 35.5 | 65 | 45 | FULL | 28 | 2 | 100 | 0.28 |
| TY125 | 1-1/4 | 31.8 | 1.63 | 41.4 | 60 | 40 | FULL | 28 | 3 | 100 | 0.33 |
| TY150 | 1-1/2 | 38.1 | 1.93 | 49.0 | 50 | 35 | FULL | 28 | 3 | 100 | 0.44 |
| TY200 | 2 | 50.8 | 2.51 | 63.8 | 50 | 35 | FULL | 28 | 5 | 100 | 0.67 |
| TY300 | 3 | 76.2 | 3.60 | 91.5 | 45 | 30 | FULL | 26 | 7 | 100 | 1.14 |
| TY400 | 4 | 101.6 | 4.70 | 119.5 | 40 | 25 | FULL | 26 | 11.5 | 100 | 1.84 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

NOTE: Contact your nearest KOA warehouse for availability of 50 ft. lengths.

*Actual service temperature range is application dependent.

Tiger™ Red TRED™  Series

# Tiger™ Blue TBLU™  Series

## EPDM Suction Hoses

### General Applications:

##### Agriculture liquid fertilizers

  - Irrigation lines

  - Liquid manure handling

  - Marine bilge discharge

  - Pumps, rental and construction dewatering

  - Pumps, trash

  - Septic and wastewater handling

  - Used frack solution removal

  - Water suction – standard duty

Construction: EPDM tube with polyethylene helix.

Service Temperature: -40°F (-40°C) to 160°F (+71°C)*

### Features and Benefits:

  - Superior Rubber Compounds – Tigerflex™ uses only the best available EPDM compounds, which provide the ideal combination of light-weight, flexibility, durability and chemical resistance.

  - Superior Flexibility – Our tests show up to 22% more flexible than the competition, especially in sub-zero weather! Tiger™ Green comes off the trucks more flexible and easier to handle than other similar hoses.

TRED

TBLU

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces and around corners. Easy-to-handle.

- Convoluted Outer Cover – Provides increased hose flexibility.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Color Choices – Choose from colors red or blue to match company equipment.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| TRED/TBLU200 | 2 | 50.8 | 2.51 | 63.8 | 50 | 35 | FULL | 28 | 5 | 100 | 0.67 |
| TRED/TBLU300 | 3 | 76.2 | 3.60 | 91.5 | 45 | 30 | FULL | 26 | 7 | 100 | 1.14 |
| TRED/TBLU400 | 4 | 101.6 | 4.70 | 119.5 | 40 | 25 | FULL | 26 | 11.5 | 100 | 1.84 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

Tiger™ TSD™ Series

## EPDM Fabric Reinforced Suction & Discharge Hose

G

• Agricultur

• Agri-foam

eneral Applications:

##### e liquid fertilizers systems

  - Liquid manure handling

  - Pumps, rental and construction dewatering

  - Pumps, trash

  - Septic and wastewater handling

  - Suction and discharge

  - Water suction – heavy duty

Construction: Double-ply EPDM, polyester fabric reinforcement and polyethylene helix.

Service Temperature: -40°F (-40°C) to 160°F (+71°C)*

### Features and Advantages:

- Superior Rubber Compounds – Tigerflex™ uses only the best available EPDM compounds, which provide the ideal combination of light-weight, flexibility, durability and chemical resistance.

- Fabric Reinforcement – Designed with high tensile strength polyester yarn jacket to handle both suction, and higher pressure discharge applications.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Easy Slide Helix – Rigid helix design protects hose tube from cover wear, and allows hose to slide easily over rough surfaces and around corners. Easy-to-handle.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| TSD125 | 1-1/4 | 31.8 | 1.70 | 43.2 | 100 | 75 | FULL | 28 | 3 | 100 | 0.41 |
| TSD150 | 1-1/2 | 38.1 | 2.00 | 50.7 | 100 | 75 | FULL | 28 | 3 | 100 | 0.51 |
| TSD200 | 2 | 50.8 | 2.54 | 64.5 | 100 | 75 | FULL | 28 | 5 | 100 | 0.73 |
| TSD300 | 3 | 76.2 | 3.62 | 92.0 | 90 | 65 | FULL | 26 | 8 | 100 | 1.18 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

NOTE: Contact your nearest KOA warehouse for availability of 50 ft. lengths.

STIG™  Series

## Extremely Heavy Duty

Polyurethane Lined Material Handling Hose

### General Applications:

##### Fly ash collection

  - Industrial Vacuum Equipment

  - Material chutes

  - Material handling – heavy duty abrasive

  - Milling machine scrap recovery

NEW

Our Most Internal Abrasion Resistant Hose!

##### Rock, gravel, sand and crushed concrete vacuuming

  - Shot blast recovery

Construction: PVC cover with extra thick polyurethane liner, rigid PVC helix and grounding wire.

Service Temperature: -4°F (-20°C) to 150°F (+65°C)*

### Features and Advantages:

  - Extra Thick Abrasion Resistant Polyurethane Liner – Designed for dry applications where severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

  - Grounding Wire – Multi-strand wire helps prevent the build-up of static electricity for added safety and to help keep material flowing smoothly. It’s embedded within the rigid helix to prevent contamination of transferred materials.

- Convoluted Outer Cover – Provides increased hose flexibility.

• Oil Resistant Polyurethane Liner – Resists most animal and petroleum based oils.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg.) |  | Min. Bending Radius (in. @ 68ºF) | Standard Length (ft.) | Weight (lbs./ft.) |
|  |  |  |  |  | 68ºF | 104ºF | 68ºF | 104ºF |  |  |  |
| STIG250 | 2-1/2 | 63.5 | 3.04 | 77.2 | 45 | 22 | Full | 28 | 7 | 100 | 0.92 |
| STIG300 | 3 | 76.2 | 3.77 | 95.8 | 45 | 22 | Full | 28 | 8 | 100 | 1.50 |
| STIG400 | 4 | 101.6 | 4.86 | 123.5 | 40 | 20 | Full | 28 | 12 | 100/20 | 2.32 |
| STIG500 | 5 | 127.0 | 5.86 | 148.8 | 35 | 18 | Full | 28 | 16 | 60/20 | 3.43 |
| STIG600 | 6 | 153.4 | 7.18 | 182.4 | 35 | 18 | Full | 28 | 20 | 100/50/20 | 4.54 |
| STIG800 | 8 | 204.8 | 9.49 | 241.0 | 35 | 18 | 28 | 25 | 25 | 50/20 | 7.53 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

*Actual service temperature range is application dependent.

CAUTION: This product is designed to dissipate static electricity when the embedded grounding wire is physically extracted and securely connected to ground, through the fitting or by other means.

WOR™  Series

## Standard Duty Oil Resistant PVC Suction Hose

### General Applications:

##### Environmental clean-up

  - Oil skimming

  - Oil slurries

  - Oil suction

  - Vapor recovery – hydrocarbon emmissions

Construction: Oil resistant PVC tube with rigid PVC helix.

Service Temperature: 5°F (-15°C) to 150°F (+65°C)*

### Features and Advantages:

- Oil Resistant PVC – Made with special oil resistant compounds which exhibit medium resistance to oil and other hydrocarbons.

- Convoluted Outer Cover – Provides increased hose flexibility.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| WOR150 | 1-1/2 | 38.1 | 1.92 | 48.8 | 50 | 25 | 28 | 24 | 3 | 100 | 0.31 |
| WOR200 | 2 | 50.8 | 2.40 | 61.0 | 40 | 20 | 28 | 24 | 4 | 100 | 0.50 |
| WOR300 | 3 | 76.2 | 3.64 | 92.5 | 40 | 20 | 28 | 24 | 6 | 100 | 1.17 |
| WOR400 | 4 | 101.6 | 4.72 | 119.9 | 35 | 18 | 28 | 22 | 10 | 100 | 1.74 |

ORV™ Series

Standard Duty Oil Resistant

PVC Suction Hose

General Applications:

- Environmental cleanup

- Oil skimming

- Oil slurries

- Oil suction

- Vapor recovery – hydrocarbon emissions

Construction: Oil resistant PVC tube with rigid PVC helix.

Service Temperature: 5°F (-15°C) to 150°F (+65°C)*

### Features and Benefits:

- Oil Resistant PVC Tube – Made with special oil resistant compounds which exhibit medium resistance to oil and other hydrocarbons.

- Smooth Outer Cover – Provides increased pressure rating and smooth surface for banding.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| ORV075 | 3/4 | 19.0 | 1.01 | 25.6 | 100 | 60 | 28 | 26 | 3 | 100 | 0.19 |
| ORV100 | 1 | 25.4 | 1.26 | 32.0 | 80 | 50 | 28 | 26 | 3 | 100 | 0.24 |
| ORV150 | 1-1/2 | 38.1 | 1.76 | 44.6 | 60 | 40 | 28 | 24 | 5 | 100 | 0.35 |
| ORV200 | 2 | 50.8 | 2.32 | 59.0 | 60 | 40 | 28 | 24 | 7 | 100 | 0.55 |
| ORV300 | 3 | 76.2 | 3.41 | 86.7 | 65 | 40 | 28 | 22 | 10 | 100 | 1.09 |

NOTE: Service life may vary depending on operating conditions and type of material being conveyed.

NOTE: For details of the following compliances, refer to footnotes listed on page 62.

*Actual service temperature range is application dependent.

Oil Vac™ OV™ Series

## Heavy Duty Oil Resistant Polyurethane Suction Hose

TM

Features and Advantages:

  - Oil Resistant Polyurethane Tube – Handles most fuels and oils. Excellent resistance to gasoline, diesel, ethanol, blends (up to E30) and biodiesels (up to B100).

  - Abrasion Resistant Polyurethane Tube – Solid polyurethane tube outlasts other materials when severe abrasion is a factor. Provides for longer hose life and lower operating costs versus rubber or PVC hoses.

General Applications:

- Material handling - heavy duty abrasive

- Material chutes

- Oil suction – heavy duty

Construction: Polyurethane tube with rigid PVC helix.

Service Temperature: -40°F (-40°C) to 150°F (+65°C)*

- Transparent Construction – “See-the-flow.” Allows for visual confirmation of material flow.

- “Cold-Flex” Materials – Hose remains flexible in sub-zero temperatures.

- Phthalate Free

| Nominal Specifications |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Series | ID (in.) | ID (mm) | OD (in.) | OD (mm) | Working Pressure (psi) |  | Vacuum Rating (in. Hg) |  | Approx. Bending Radius (in. @ 68°F) | Standard Length (ft.) | Weight (lbs/ft.) |
|  |  |  |  |  | 68°F | 104°F | 68°F | 104°F |  |  |  |
| OV100 | 1 | 25.4 | 1.26 | 32.0 | 85 | 60 | 28 | 26 | 3 | 100 | 0.23 |
| OV125 | 1-1/4 | 31.7 | 1.49 | 37.8 | 85 | 60 | 28 | 24 | 5 | 100 | 0.30 |
| OV150 | 1-1/2 | 38.1 | 1.76 | 44.6 | 70 | 50 | 28 | 24 | 5 | 100 | 0.35 |
| OV200 | 2 | 50.8 | 2.32 | 59.0 | 65 | 45 | 28 | 24 | 7 | 100 | 0.55 |

  - For food grade and non-food grade applications.

  - Easy assembly.

  - Provides smoother surface for banding behind coupling.

BCCF™ Series

  - Clear, food grade, rigid PVC coils

  - For hoses with a high-profile, counterclockwise helix*

| Nominal Specifications |  |  |  |
| --- | --- | --- | --- |
| Part No. | Fits Hose ID | Color | Weight (lbs/ea.) |
| BCCF1.5 | 1-1/2" | Clear | 0.20 |
| BCCF2 | 2" | Clear | 0.30 |
| BCCF3 | 3" | Clear | 0.60 |
| BCCF4 | 4" | Clear | 0.90 |
| BCCF5 | 5" | Clear | 1.10 |
| BCCF6 | 6" | Clear | 1.30 |
| BCCF8 | 8" | Clear | 1.40 |

Food Grade, High-Profile, Counterclockwise Coils

- Packaged singly: One piece to make one complete hose assembly coupled at each end.

- Cut one piece in half into two equal pieces; thread between hose helix.

Banding Coils

Rigid PVC Coils

Accessories

BCWF™ Series

  - White, food grade, rigid PVC coils

  - For hoses with a low-profile, counterclockwise helix*

Food Grade, Low-Profile, Counterclockwise Coils

| Nominal Specifications |  |  |  |
| --- | --- | --- | --- |
| Part No. | Fits Hose ID | Color | Weight (lbs/ea.) |
| BCWF2 | 2" | White | 0.25 |
| BCWF3 | 3" | White | 0.45 |

BCRT™ Series

  - Grey, non-food grade, rigid PVC coils

  - For hoses with a high-profile, clockwise helix*

Non-Food Grade, High-Profile, Clockwise Coils

| Nominal Specifications |  |  |  |
| --- | --- | --- | --- |
| Part No. | Fits Hose ID | Color | Weight (lbs/ea.) |
| BCRT2 | 2" Grey 0.30 |  |  |
| BCRT3 | 3" Grey 0.60 |  |  |
| BCRT4 | 4" Grey 0.90 |  |  |

BCYL™ Series

  - Yellow, non-food grade, rigid PVC coils

  - For hoses with a low-profile, counterclockwise helix*

Non-Food Grade, Low-Profile, Counterclockwise  Coils

| Nominal Specifications |  |  |  |
| --- | --- | --- | --- |
| Part No. | Fits Hose ID | Color | Weight (lbs./ea.) |
| BCYL2 | 2.02" Yellow 0.25 |  |  |
| BCYL3 | 3.03" Yellow 0.45 |  |  |
| BCYL4 | 4.04" Yellow 0.75 |  |  |

BCCF

BCWF

BCRT

BCYL

*Refer to Tigerflex Accessories compatability chart on page 59-61.

SLV-VLT

SLV-DRP

SLV-VAP

SLV-NDH

Flexible PVC Sleeves

- Helps prevent overbending near the coupling.

• Ph

Cut into approximately 12-inch lengths; screw onto hose at each end. thalate Free

SLV-VLT™ Series

  - Clear, food grade, static dissipative PVC

  - For hoses with a high-profile, counterclockwise helix*

| Nominal Specifications |  |  |  |
| --- | --- | --- | --- |
| Part No. | Fits Hose ID | Color | Weight (lbs/ea.) |
| SLV-VLT3X3 | 3" | Clear | 3.50 |
| SLV-VLT4x3 | 4" | Clear | 4.29 |

SLV-DRP™ Series

  - Green, non-food grade flexible PVC

  - For hoses with a high-profile, counterclockwise helix*

| Nominal Specifications |  |  |  |
| --- | --- | --- | --- |
| Part No. | Fits Hose ID | Color | Weight (lbs/ea.) |
| SLV-DRP3X3 | 3" | Green | 3.06 |
| SLV-DRP4X3 | 4" | Green | 4.29 |

SLV-VAP™ Series

  - Yellow, non-food grade flexible PVC

  - For hoses with low-profile, counterclockwise helix*

| Nominal Specifications |  |  |  |
| --- | --- | --- | --- |
| Part No. | Fits Hose ID | Color | Weight (lbs/ea.) |
| SLV-VAP2X3 | 2" Yellow 1.80 |  |  |
| SLV-VAP3X3 | 3" Yellow 3.09 |  |  |
| SLV-VAP4X3 | 4" Yellow 4.20 |  |  |

SLV-NDH™ Series

  - Grey, non-food grade flexible PVC

| Nominal Specifications |  |  |  |  |
| --- | --- | --- | --- | --- |
| Part No. | Fits Hose ID | Color | Standard Length (ft.) | Weight (lbs./ea.) |
| SLV-NDH2X3 | 2.02" Grey 3 1.83 |  |  |  |
| SLV-NDH3X3 | 3.03" Grey 3 3.06 |  |  |  |
| SLV-NDH4X3 | 4.04" Grey 3 4.29 |  |  |  |

For hoses with high-profile, clockwise helix*

Banding Sleeves

Accessories

*Refer to Tigerflex Accessories compatability chart on pages 59-61.

- Zinc plated carbon steel.

TigerClamps™

Accessories

Spiral Double Bolt Clamps

- Two or more TigerClamps™ are suggested for 3” ID and larger hoses.

- Both hex nuts should be tightened equally to prevent leakage.

- Caution: proper evaluation of holding power for each clamp must be determined for each individual application.

For Counterclockwise Helix Hoses

Designed to fit most Tigerflex Hoses*

| Nominal Specifications |  |  |  |
| --- | --- | --- | --- |
| Part No. | Fits Hose (ID) | Weight ea. (lbs.) | Standard Carton Qty. |
| SDBC-1.5 | 1-1/2" | 0.18 | 100 |
| SDBC-2 | 2" | 0.36 | 100 |
| SDBC-2.25 | 2-1/4" | 0.40 | 100 |
| SDBC-2.5 | 2-1/2" | 0.48 | 100 |
| SDBC-3 | 3" | 0.66 | 70 |
| SDBC-3.5 | 3-1/2" | 0.70 | 70 |
| SDBC-4 | 4" | 1.02 | 40 |
| SDBC-5 | 5" | 1.76 | 30 |
| SDBC-6 | 6" | 2.00 | 20 |
| SDBC-8 | 8" | 2.76 | 10 |
| SDBC-10 | 10" | 3.46 | 10 |
| SDBC-12 | 12" | 4.14 | 10 |

For Clockwise Helix Hoses

Nominal Specifications

Designed to fit Tigerflex TR1 and THT-series hoses*

|  | Fits | Weight ea. Standard |  |
| --- | --- | --- | --- |
| Part No. | Hose (ID) | (lbs.) | Carton Qty. |
| SDBCR-1.5 | 1.5" | 0.18 | 100 |
| SDBCR-2 | 2" | 0.36 | 100 |
| SDBCR-3 | 3" | 0.66 | 70 |
| SDBCR-4 | 4" | 1.02 | 40 |
| SDBCR-5 | 5" | 1.76 | 30 |
| SDBCR-6 | 6" | 2.00 | 20 |
| SDBCR-8 | 8" | 2.76 | 10 |
| SDBCR-10 | 10" | 3.46 | 10 |
| SDBCR-12 | 12" | 4.14 | 10 |

*Refer to Tigerflex Accessories compatability chart on pages 59-61.

TigerClamp™ Stainless Steel Spiral Double Bolt Clamp

(For Counterclockwise Spiral)

Nominal Specifications

Fits	Weight ea.

Standard

Designed to Fit Tigerflex™ PVC Suction Hoses

| Part No. | Hose (ID) | (lbs.) | Carton Qty. |
| --- | --- | --- | --- |
| SDBC-SS-1.5 | 1 1/2" | 0.40 | 100 |
| SDBC-SS-2 | 2" | 0.42 | 100 |
| SDBC-SS-2.5 | 2.5" | 0.53 | 100 |
| SDBC-SS-3 | 3" | 0.88 | 50 |
| SDBC-SS-3.5 | 3.5" | 0.77 | 70 |
| SDBC-SS-4 | 4" | 1.01 | 40 |
| SDBC-SS-6 | 6" | 2.09 | 20 |
| SDBC-SS-8 | 8" | 2.97 | 10 |

Threaded protective cap for safety

| Tigerflex™ Accessories Compatability Chart |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| G = Suggested -- = Not Suggested | Series | Banding Coils BCCF BCWF BCRT |  |  | Banding Sleeves SLV-VLT SLV-DRP SLV-VAP |  |  | Clamps SDBC SDBC-R |  | Cuff A2150L1 |  |
|  | 2001-200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | 2001-300 | G | G | -- | -- | -- | -- | G | -- | -- |  |
|  | 2001-400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | 2001 other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | 2020-300 | G | -- | -- | -- | G | -- | G | -- | -- |  |
|  | 2020-400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | 2020 other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | AMPH400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | AMPH other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | BARK400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | BARK500 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | BW500 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | BW600 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | BW other sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | CF200 | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | CF300 | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | CF400 | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | CF600 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | CF other sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | F600 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | F800 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | F other sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | FT all sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | G600 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | G800 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | G other sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | GC-C400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | GC-C500 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | GC-C600 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | GT/GTG/GTFE150 | G | -- | -- | -- | -- | -- | G | -- | G |  |
|  | GT/GTG/GTFE200 | -- | G | -- | -- | -- | G | G | -- | -- |  |
|  | GT/GTG/GTFE300 | -- | G | -- | -- | -- | G | G | -- | -- |  |
|  | GT/GTG/GTFE400 | G | -- | -- | -- | -- | G | G | -- | -- |  |
|  | GT/GTG/GTFE other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | H600 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | H800 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | H other sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | J600 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | J800 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | J other sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | K600 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | K800 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | K other sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | LK/LKC300 | G | -- | -- | -- | -- | G | G | -- | -- |  |
|  | LK/LKC400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | LK/LKC other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |

NOTE: Banding coils and sleeves must be used in conjunction with a suitable hose clamp.

Refer to individual accessory pages in our Kuriyama-Couplings™ Catalog for detailed information on size availability.

| Tigerflex™ Accessories Compatability Chart |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| G = Suggested -- = Not Suggested | Series | Banding Coils BCCF BCWF BCRT |  |  | Banding Sleeves SLV-VLT SLV-DRP SLV-VAP |  |  | Clamps SDBC SDBC-R |  | Cuff A2150L1 |  |
|  | MH150 | -- | -- | -- | -- | -- | -- | G | -- | G |  |
|  | MH200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | MH other sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | MILK | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | MILK-LT | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | MULCH400 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | MULCH500 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | MULCH600 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | ORV all sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | OV all sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | PF300 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | PF400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | PF other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | S300 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | S400 | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | S other sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | SH300 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | SH400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | SH other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | TG/TY/TRED/TBLU all sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | TR1-200 | -- | -- | G | -- | -- | -- | -- | G | -- |  |
|  | TR1-300 | -- | -- | G | -- | -- | -- | -- | G | -- |  |
|  | TR1-400 | -- | -- | G | -- | -- | -- | -- | G | -- |  |
|  | TR1 other sizes | -- | -- | -- | -- | -- | -- | -- | G | -- |  |
|  | TSD all sizes | -- | -- | -- | -- | -- | -- | -- | -- | -- |  |
|  | UBK200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | UBK300 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | UBK400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UBK other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UF1-200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | UF1-300 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UF1-400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UF1 other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UF2-200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | UF2-300 | G | -- | -- | -- | G | -- | G | -- | -- |  |
|  | UF2-400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | UF2 other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UFC200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | UFC300 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | UFC400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UV1/UVF150 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UV1/UVF200 | -- | G | -- | -- | -- | G | G | -- | -- |  |
|  | UV1/UVF300 | -- | G | -- | -- | -- | G | G | -- | -- |  |
|  | UV1/UVF400 | G | -- | -- | -- | -- | G | G | -- | -- |  |
|  | UV2-200 | G | -- | -- | -- | -- | G | G | -- | -- |  |
|  | UV2-400 | G | G | X | X | X | G | G | X | X |  |

NOTE: Banding coils and sleeves must be used in conjunction with a suitable hose clamp.

Refer to the individual accessory pages in our Kuriyama-Couplings™ Catalog for detailed information on size availability.

CAUTION NOTE: This chart is provided only as a guideline for selection of hose accessories. Actual results will vary due to manufacturing tolerances.

| Tigerflex™ Accessories Compatability Chart |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| G = Suggested -- = Not Suggested | Series | Banding Coils BCCF BCWF BCRT |  |  | Banding Sleeves SLV-VLT SLV-DRP SLV-VAP |  |  | Clamps SDBC SDBC-R |  | Cuff A2150L1 |  |
|  | UV1/UVF/UVE other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UV2-300 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UV2 other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UV3-300 | G | G | -- | -- | -- | G | G | -- | -- |  |
|  | UV3-400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UV3 other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | UVPE all sizes | -- | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | VOLT200 | G | -- | -- | -- | -- | G | G | -- | -- |  |
|  | VOLT300 | G | G | -- | -- | -- | G | G | -- | -- |  |
|  | VOLT400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | VOLT other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | VLT-SD300 | G | -- | -- | -- | G | -- | G | -- | -- |  |
|  | VLT-SD400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | VLT-SD other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | W200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | W300 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | W400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | W other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | WBS200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | WBS300 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | WBS400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | WBS other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | WE200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | WE300 | -- | G | -- | -- | G | -- | G | -- | -- |  |
|  | WE400 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | WE other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | WG200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | WG300 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | WG400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | WG other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | WH200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | WOR150 | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | WOR200 | -- | G | -- | -- | -- | G | G | -- | -- |  |
|  | WOR300 | G | G | -- | -- | G | -- | G | -- | -- |  |
|  | WOR400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | WST/WSTF300 | G | G | -- | -- | G | -- | G | -- | -- |  |
|  | WST/WSTF400 | G | G | -- | G | G | -- | G | -- | -- |  |
|  | WST/WSTF other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |
|  | WT200 | -- | G | -- | -- | -- | -- | G | -- | -- |  |
|  | WT300 | G | G | -- | -- | -- | -- | G | -- | -- |  |
|  | WT400 | G | -- | -- | G | G | -- | G | -- | -- |  |
|  | WT other sizes | G | -- | -- | -- | -- | -- | G | -- | -- |  |

NOTE: Banding coils and sleeves must be used in conjunction with a suitable hose clamp.

Refer to the individual accessory pages in our Kuriyama-Couplings™ Catalog for detailed information on size availability.

Quality Assurance

ISO 9001 Registration

Tigerflex™ hoses are manufactured with ISO 9001 registered quality management systems.

The ISO 9001 family of standards represents an international consensus on good manufacturing practices with the aim of ensuring that the organization consistently delivers the product or services that meet the customer’s quality requirements.

ISO 9001 is a quality assurance model against which a plant’s quality system can be independently audited.

Compliance Footnotes for Tigerflex™ Catalog Products

3A – Material approved by 3-A Sanitary Standards, Inc. for multi-use plastic materials, number: 20-25, as product contact surfaces in equipment for production, processing and handling of milk and milk products.

  - BSE/TSE – The majority of the raw materials used in our formulations are not manufactured or derived from materials of animal origin. Nor do our products come into contact with materials of animal origin during processing. Our suppliers of raw materials have assured

us their compounds exceed the relevant European Guidance on minimizing the Risk of Transmitting Animal Spongiform Encephalophy Agents Via Human and Veterinary Medical Products.

  - FDA – Material conforms to CFR title 21, parts 170-199.

  - FDA – Material conforms to CFR title 21, parts 177.1680 and 177.2600.

  - FDA – Material conforms to CFR title 21, parts 177.2600 and 175.105.

  - FDA – Material conforms to CFR title 21, parts 177.2800 (5)(i), 21 CFR 170.39.

  - MSHA – Hose approved by the United States Department of Labor’s Mine Safety and Health Administration as having met Part 18, Title 30 CFR, and the Interim Fire Criteria for Acceptance of Products Taken into Underground Mines as water transfer hose.

  - MSHA – Hose approved by the United States Department of Labor’s Mine Safety and Health Administration as having met the Interim Fire Criteria Acceptance of Products Taken Into Underground Mines as a hydraulic hose/hose bundle protection sleeve. Not intended for protection of electrical cables, and not intended for the repair or conveying of damaged hydraulic hoses.

  - Phthalate Free – Manufactured from all phthalate free materials.

- RoHS – The product complies with the requirements of the EU directive 2002/95/EC which is on the restriction of the use of certain hazardous substances in electrical and electronic equipment.

- USDA – Hose approved by the US Department of Agriculture for use in federally inspected meat and poultry plants.

Because we continually examine ways to improve our products, we reserve the right to alter specifications or discontinue products without prior notice.

62	KTFC0218

Flexibility

The terms Flexibility and Minimum Bend Radius are often used interchangeably. However, while closely related, their meanings are different.

Minimum Bend Radius is generally defined as the smallest radius to which a hose can be bent without damage. Tiger- flex™ defines damage as a 5% reduction of the hose OD at the bend point (before kinking/collapse). Other manufactur- ers may define damage as complete hose kinking/collapse.

| Food Grade |  |  |  |
| --- | --- | --- | --- |
| Series | Force to Bend (Lbs./F) * |  |  |
|  | 2” ID x 3 ft. | 3” ID x 5 ft. | 4” ID x 7 ft. |
| GTF/GTFE | 0.3 | 0.8 | 3.5 |
| UVF | 2.5 | 3.6 | 5.5 |
| WT | 4.5 | 6.5 | 16.0 |
| WE | 5.5 | 8.8 | 21.4 |
| 2001 | 5.6 | 9.0 | 21.0 |
| PF | - | 13.0 | 19.0 |
| WBS | 5.5 | 13.1 | 22.0 |
| WSTF | - | 14.0 | 22.0 |
| VOLT | 7.8 | 15.0 | 22.0 |
| MILK-LT | 10.0 | 15.0 | - |
| MILK | 11.0 | 17.0 | - |
| FT | 13.0 | 24.0 | 41.0 |
| 2020 | - | 31.0 | 41.0 |
| VLT-SD | - | 33.0 | 42.4 |

| Ducting |  |  |  |
| --- | --- | --- | --- |
| Series | Force to Bend (Lbs./F) * |  |  |
|  | 2” ID x 3 ft. | 3” ID x 5 ft. | 4” ID x 7 ft. |
| CG/CG-SL | 0.5 | 1.2 | 2.1 |
| GT/GTG | 0.5 | 1.5 | 2.8 |
| LK/LKC | - | 1.8 | 3.0 |
| UV1/UVE | 3.0 | 3.7 | 5.5 |

| Liquid Suction |  |  |  |
| --- | --- | --- | --- |
| Series | Force to Bend (Lbs./F) * |  |  |
|  | 2” ID x 3 ft. | 3” ID x 5 ft. | 4” ID x 7 ft. |
| WH/SH | 2.8 | 2.5 | 3.5 |
| MH | 2.8 | - | - |
| WOR | 2.8 | 5.3 | 10.0 |
| W | 4.0 | 9.5 | 7.3 |
| WG | 4.5 | 10.0 | 15.0 |
| BW | 7.8 | 12.3 | 19.5 |
| ORV | 10.0 | 12.0 | - |
| TG/TY | 12.0 | 11.2 | 22.0 |
| TRED/TBLU | 12.0 | 11.2 | 22.0 |
| WST | - | 14.0 | 21.0 |
| CF | 14.5 | 14.0 | 28.5 |
| TSD | 14.8 | 18.8 | - |
| H/J/K | 12.1 | 24.0 | 34.0 |
| OV | 19.0 | 29.0 | - |
| S | 24.6 | 29.0 | 35.5 |
| F/G | 26.0 | 31.0 | 47.0 |

Flexibility is defined as the amount of force required in order to bend the hose to a specified radius without kinking. In order to provide a better understanding of the flexibility of Tigerflex™ hoses we’ve performed extensive force-to-bend testing. This data provides a clearer picture of the actual flexibility of our hoses in order to assist in your hose selection process.

| Material Handling |  |  |  |
| --- | --- | --- | --- |
| Series | Force to Bend (Lbs./F) * |  |  |
|  | 2” ID x 3 ft. | 3” ID x 5 ft. | 4” ID x 7 ft. |
| UV2 | 3.4 | 5.5 | 7.0 |
| BARK | - | - | 7.6 |
| MULCH-LT | - | - | 8.0 |
| TR1 | 3.4 | 5.0 | 8.0 |
| GC-C | - | - | 9.0 |
| UBK | 6 | 8 | 11.5 |
| UV3 | - | 7.0 | 13.0 |
| UFC | 4.8 | 8.0 | 12.2 |
| UF1 | 4.8 | 8.0 | 12.2 |
| UVPE | 5.5 | 7.5 | - |
| AMPH | 5.5 | 10.0 | 15.5 |
| UF2 | 5.5 | 10.1 | 17.2 |
| MULCH | - | - | 18.2 |

A lower force-to-bend value indicates a more flexible hose.

*Values listed indicated pounds of force required to bend a straight length of hose to 180º at 68ºF.

These recommendations are based on our laboratory test reports which are, to the best of our knowledge, complete and accurate. However, actual hose force-to-bend requirements can vary due to many factors such as hose age and manufacturing tolerances. Therefore, no guarantee is expressed or implied by our publication of this chart. If doubt exists, we advise that a sample of the hose in question be obtained and tested under actual conditions. These values are provided for reference only and are subject to change.

Hoses have a limited service life and users must be alert to signs of impending failure. Users of industrial hose should have safety and inspection procedures in place. Hose users should be trained how to properly inspect a hose for signs of impending failure. Hose should be routinely inspected for signs of damage.

Length of hose service life is affected by several factors includ- ing the type of material conveyed, pressure, vacuum, number and degree of bends, amount of flexing and

exposure to environmental elements. Since we have no control over the way in which the hose is used, we do not warrant our hose for any particular service life.

Hoses and fittings should be routinely inspected for signs of damage, such as:

- Cuts, cracks, severe abrasions or holes in the hose tube, helical support or grounding wire

- Ovaling, kinking, bulging or any other deformation of the hose’s normal shape

- Hardening or soft spots

- Flaking or chipping

- Misalignment or weakening of the coupling retention

- Fitting or clamp damage such as loose clamps, missing pins, worn threads excessive corrosion

If any of these signs of damage are observed, contact your hose supplier for replacement or repair.

Care and Maintenance

Recommended Practices

Hoses should only be used to convey materials compatible with hose construction. Refer to the Chemical Resistance and Application Guides in this catalog.

Hoses should not be used at levels that exceed their working pressure or vacuum ratings, and should not be subjected to severe pressure spikes or abrupt drops in pressure.

Hoses can sustain damage at high temperatures. Care should be exercised to not exceed the temperature limits of the hose. Hose should not be installed near sources of high heat.

Do not subject hose to abuse during service. Hose should not be thrown, dropped or subjected to severe impacts.

Machinery should not be moved by pulling on the hose. Protect the hose from sharp edges and corners by using

appropriate hose covers or sleeves.

If hose is used in a suspended position it should be supported in multiple points with use of proper hose slings in order to evenly distribute the hose weight.

Hose should not be used in applications where hose failure would result in contents exposure to open flame or other igni- tion sources.

When not in service hoses should be drained and stored prop- erly.

Storage and Handling

The following storage conditions and handling procedures can enhance and substantially extend the ultimate life of Tigerflex™ hose.

Upon receipt of Tigerflex™ product, skids should be broken down and product inspected for shipping damage. Skids are configured for shipping purposes only.

Hose should be stored indoors out of direct sunlight. Hose should be stored a minimum of ten feet from fluorescent light fixtures.

Hose should always be stored flat on smooth surfaces. Hose should not be stored on its side as this can cause the section of the hose resting on the ground to become deformed, or “egg shaped”.

Hose coils should not be stacked more than six coils high. Larger diameter hoses, 4” and above, should be stacked fewer than six coils high. Please refer to the following chart for recommended maximum stacking height requirements by hose size:

| Hose Size (ID) | 3/4” | 1” | 1-1/4” | 1-1/2” | 2” | 2-1/2” | 3” | 4” | 5” | 6” | 8”+ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Max Coil Stack Height | 6 | 6 | 6 | 6 | 6 | 6 | 6 | 5 | 3 | 2 | 1 |

Exceeding these coil stacking requirements may cause the compression load factor on the bottom coil to exceed the hose’s load limitations, causing the bottom coil to flatten out.

Hose should be pulled from inventory on a first-in, first-out (FIFO) basis.

During storage, hose should be kept in its original wrapping when possible, and kept free of dust and dirt.

Hose should not be exposed to water, oils, solvents, or corrosive liquids and fumes during storage. Hose should be protected from rodents and insects.

Rubber hoses should not be stored near electrical equipment. The motor in the equipment can generate ozone, which can attack and damage rubber hose.

Hose should not be subjected to extreme temperatures. Ideal hose storage temperature is between 50°F and 70°F, and ideally should not exceed 100°F. Be aware, when the air temperature is over 90°F outdoor ground surfaces such as asphalt, concrete and gravel can be in excess of 150°F. Such extreme heat conditions could reduce service life of thermoplastic products. Do not store hoses near heat sources such as heat vents, heaters or radiators. Hoses should not be exposed to dampness or high humidity during storage.

Hose should not be kinked or run over by any equipment. Do not drag the hose during storage & shipping. In the handling of larger ID hose, dollies should be used in transporting whenever possible. Slings or handling rigs, properly placed in multiple locations throughout the hose, should be used to support heavier hose. Hanging and supporting coils using forklift forks without protection may damages hose.

The Effect of Temperature

on Working Pressure & Vacuum Ratings

As a general rule, the working pressure and vacuum ratings for plastic reinforced hoses are based

on room temperature conditions. The maximum allowable working pressure or vacuum/suction for a hose decreases as the temperature increases and the material becomes softer and more elastic. Excessive bending of a hose while in service can

Working Pressure Ratings

Pressure and vacuum hose strength decreases as temperature increases

Working pressure and vacuum ratings are given in this catalog at 68°F and 104°F. Between 104°F and the maximum service temperature, it must be noted that a rapid decline in the pressure or vacuum rating of the hose may occur, and all factors relating to the hose, fittings and service conditions must be taken into consideration.

also affect the allowable service application working pressure and vacuum.

Working pressure and vacuum ratings can be affected significantly by the type of fitting used, the method of attachment, and the temperature to which the hose assembly is exposed in service. The graph below demonstrates the overall trend.

No warranty is expressed or implied, as applications and methods of fitting installation may vary widely. Before placing a hose in service, the user must determine the suitability of the product under the correct working conditions, and assumes all risk and liability in connection therewith.

Many new materials have been developed to handle the wide range of modern chemicals being used

in industry today. Many of these materials are now being used in the construction of Tigerflex™ hose.

The Chemical Resistance Guides which appears on the following pages have been prepared to assist the user in the selection of the correct hose for the application.

These recommendations are based on laboratory and test reports which are, to the best of our knowledge, complete and accurate. However, the degree of chemical resistance of any given material depends upon many variables, including  such factors as length of exposure, temperature, pressure, fluid velocity, and chemical concentration.

Therefore, no guarantee is expressed or implied by our publication of these Chemical Resistance

Guides. If an element of doubt exists, we advise that a sample of the specific hose selected be obtained and tested under actual conditions.

Furthermore, listings in these Chemical Resistance Guides do not imply conformance to any U. S. Department of Agriculture (USDA), Food and

Drug Administration (FDA) or any other federal, provincial or state laws which may be applicable when handling food products.  For information on the conformance of any specific hose product with FDA, USDA, or 3-A Sanitary Standards, please refer to the notes accompanying the information and specifications for each hose featured in this catalog.

Warning

The Chemical Resistance Guides shown on the following pages are intended for general guidance only. The information contained therein is based upon tests we believe to be reliable, but the  accuracy or completeness thereof is not guaranteed. No warranty is expressed or implied, as specific application parameters, such as temperature,

pressure and chemical concentrations vary widely. Furthermore, use of these hoses for handling multiple chemical products, either singly or as

a mixture, may introduce uncontrollable factors relating to chemical resistance.

Chemical Resistance Guides

Before using any hose, the user is responsible for determining the suitability of the hose for the intended application. Therefore, the user assumes all risk and responsibility for determining the suitability of any hose for handling any chemical or chemicals.

PVC and Polyurethane Chemical Resistance Guide

| Material Handled | Hose Materials of Construction and Temperatures |  |  |  |
| --- | --- | --- | --- | --- |
|  | PVC |  | Thermoplastic Polyurethane |  |
|  | 68°F | 104°F | 68°F | 104°F |
| Acetaldehyde Acetaldehyde 40 Pct. Acetate Solvents-Crude Acetate Solvents-Pure Acetic Acid 0-10 Pct. Acetic Acid 10-20 Pct. | U — U U G G | U — U U L L | U — L L U U | U — U U U U |
| Acetic Acid 20-30 Pct Acetic Acid 30-60 Pct. Acetic Acid 80 Pct. Acetic Acid Vapors Acetic Acid-Glacial Acetic Anhydride | G G L G L U | L L L G U U | U U U U U U | U U U U U U |
| Acetone Acetylene Acrylonitrile Adipic Acid Alcohol (See Type) Allyl Alcohol 96 Pct. | U E E G — U | U E G L — U | L E — U — U | U E — U — U |
| Allyl Chloride Alum Aluminum Acetate Aluminum Chloride Aluminum Fluoride Aluminum Hydroxide | L E G E E E | L E L E E L | U E — L E G | U E — L E L |
| Aluminum Nitrate Aluminum Oxalate Aluminum Oxychloride Aluminum Sulfate Ammonia – Aqueous Ammonia – Dry Gas | E — E E L L | E — E E U U | E — — E L L | E — — E U U |
| Ammonia-Liquid Ammoniated Latex Ammonium Bicarbonate Ammonium Carbonate Ammonium Chloride Ammonium Fluoride 25 Pct. | U E — E E U | U L — E E U | L — — E G L | U — — E L U |
| Ammonium Hydrosulphide Ammonium Hydroxide 28 Pct. Ammonium Metaphosphate Ammonium Nitrate Ammonium Persulfate Ammonium Phosphate | — G E E E | — G E E E | — L G G G | — U G G G |
| (Ammoniacal) Ammonium Phosphate-Neutral Ammonium Sulfate Ammonium Sulfide Ammonium Thiocyanate Amyl Acetate | — E E E E U | — E E E E U | — G E E G U | — G E E G U |
| Amyl Alcohol Amyl Chloride Aniline Aniline Chlorohydrate Aniline Hydrochloride Aniline Sulphate | L U L U U — | U U U U U — | U — U U U — | U — U U U — |
| Animal Oils Anthraquinone Anthraqunonesulfonic Acid Antimony Pentaculcride Antimony Trichloride Apple (Sauce or Juice) | E E E — E E | G E E — E E | — — U — E — | — — U — E — |
| Aqua Regia Aromatic Hydrocarbons Arsenic Acid 80 Pct. Arylsulfonic Acid Asphalt ASTM Fuel #1 Oil | L U E L U G | U U G U U L | U — U U E E | U — U U E E |
| ASTM Fuel #3 Oil ASTM Fuel A ASTM Fuel B ASTM Fuel C Baby Food Barium Carbonate | L G U U E E | U L U U E E | E E G G — E | E E L L — E |
| Barium Chloride Barium Hydroxide Barium Sulfate Barium Sulfide | E E E E | E E E E | E G E E | E L E E |

| Material Handled | Hose Materials of Construction and Temperatures |  |  |  |
| --- | --- | --- | --- | --- |
|  | PVC |  | Thermoplastic Polyurethane |  |
|  | 68°F | 104°F | 68°F | 104°F |
| Barley Beer Beet-Sugar Liquor Benzaldehyde Benzene Benzene-Sulfonic Acid 10 Pct. | E E E U U E | U E E U U E | — — — U L U | — — — U U U |
| Benzoic Acid Benzol Benzyl Alcohol Berries Bismuth Carbonate Black Liquor (Paper industry) | G U — E E E | L U — E E E | U L — — E — | U U — — E — |
| Bleach-12.5 Pct. Active CL Borax Bordeaux Mixture Boric Acid Boron Trifluoride Brine | G E E E E E | L G E E E E | L E — U E G | U E — U E U |
| Bromic Acid Bromine-Liquid Bromine-Water Brussel Sprouts Butadiene Butane | E U U E L E | L U U E U E | U U U — — E | U U U — — E |
| Butanediol Butanol-Primary Butanol-Secondary Butter Butyl Acetate Butyl Alcohol | — U U G U E | — U U L U L | — L L — L L | — U U — U U |
| Butyl Cellosolve Butyl Phenol Butylene Butynedial (Erythritol) Butyraldehyde Butyric Acid 20 Pct. | U L E U — L | U U G U — U | — — E U — L | — — E U — U |
| Calcium Bisulfite Calcium Carbonate Calcium Chlorate Calcium Chloride Calcium Hydroxide Calcium Hypochlorite | E E E E E E | E E E E E E | E E G L G U | E E L U L U |
| Calcium Nitrate Calcium Phosphate Calcium Sulfate Camphor Oil Cane Sugar Liquors Carbon Bisulfide | E — E — E U | E — E — E U | E — E — — — | E — E — — — |
| Carbon Dioxide (Aqueous Solution) Carbon Dioxide Gas (Wet) Carbon Disulphide Carbon Monoxide Carbon Tetrachloride Carbonic Acid | E E U E U E | E E U E U E | E E — E L U | E E — E U U |
| Carrots Casein Castor Oil Catsup Caustic Potash Caustic Soda | E E E E E L | E G E G E L | — E E — L L | — E E — U U |
| Cellosolve Cheese Cherries Chloracetic Acid Chloral Hydrate Chloric Acid 20 Pct. | L E E E E E | U G E U E E | G — — U G U | L — — U L U |
| Chlorinated Hydrocarbons Chlorine Gas (Dry) Chlorine Gas (Moist) Chlorine Water 2 Pct. Chlorine Water Saturated Chlorobenzene | U E L L — U | U E U U — U | — U U L — U | — U U U — U |
| Chloroform Chlorsulfonic Acid Chocolate Chrome Alum | U L G E | U U L E | U U — E | U U — E |

Key: E — Excellent	G — Good	L — Limited	U — Unsatisfactory

PVC and Polyurethane Chemical Resistance Guide

| Material Handled | Hose Materials of Construction and Temperatures |  |  |  |
| --- | --- | --- | --- | --- |
|  | PVC |  | Thermoplastic Polyurethane |  |
|  | 68°F | 104°F | 68°F | 104°F |
| Chromic Acid 10 Pct. Chromic Acid 25 Pct. Chromic Acid 30 Pct. Chromic Acid 40 Pct. Chromic Acid 50 Pct. Chromic Acid Plating Solution | G G L L L — | L L U U U — | U U U U U U | U U U U U U |
| Cider Citric Acid Coal Tar Coconut Oil Cola Drinks Copper Chloride | — E U L E E | — E U U E G | — U U E — E | — U U E — E |
| Copper Cyanide Copper Fluoride 2 Pct. Copper Nitrate Copper Sulfate Core Oils Corn Oils | E E E E E E | E E G G E G | — E E E E — | — E E E E — |
| Cottonseed Oil Creosote Cresol Cresylic Acid 50 Pct. Crude Oil-Sour Crude Oil-Sweet | G U U U E E | L U U U E E | E — L U E E | E — U U E E |
| Cyclohexane Cyclohexanol Cyclohexanone Demineralized Water Detergents, Synthetic Developers, Photographic | L U U E E E | U U U E G E | — L U G — — | — U U U — — |
| Dextrin Dextrose Di-acetone Alcohol Di-isodecyl Phthalate Diazo Salts Dibutyl Phthalate | E E — U E U | E G — U E U | E E — — — — | E E — — — — |
| Dichlorobenzene Diesel Oils Diethyl Ether Diethyl Ether Diethylene Glycol Diglycolic Acid | U L — L E E | U U — U E G | — — — — — — | — — — — — — |
| Dimethylamine Dioctyl Phthalate Diotylphthalate Disodium Phosphate Distilled Water Eggs (yolks or white) | U U U E E E | U U U E E E | U — G E G — | U — L E U — |
| Emulsifiers Emulsions, Photographic Ethers Ethyl Acetate Ethyl Acrylate Ethyl Alcohol | E E U U U G | E E U U U L | — — G L — — | — — L U — — |
| Ethyl Alcohol 0-50 Pct. Ethyl Alcohol 50-98 Pct. Ethyl Butyrate Ethyl Chloride Ethyl Ether Ethyl Formate | G L — U U — | L U — U U — | G L — U G — | L U — U L — |
| Ethylene Bromide Ethylene Dichloride Ethylene Glycol Ethylene Oxide Fatty Acids Ferric Chloride | E U E U E E | U U E U G E | U U G U G G | U U L U L L |
| Ferric Nitrate Ferric Sulfate Ferrous Ammonium Citrate Ferrous Chloride Ferrous Sulfate Figs | E E — E E E | E E — E E E | E E — E E — | E E — E E — |
| Fish Solubles Fixing Solution Photographic Flour Fluorine Gas-Dry | E E E U | E G U U | E — — U | G — — U |

| Material Handled | Hose Materials of Construction and Temperatures |  |  |  |
| --- | --- | --- | --- | --- |
|  | PVC |  | Thermoplastic Polyurethane |  |
|  | 68°F | 104°F | 68°F | 104°F |
| Fluorine Gas-Wet Fluoroboric Acid Fluorosilicic Acid Fluorosilicic Acid 40 Pct. Fluorosilicic Acid Concentrate Food Products, such as Milk, Buttermilk, | U E E — — | U E E — — | U E U — — | U E U — — |
| Molasses, Salad Oils, Fruit Foric Acid Formaldehyde 40 Pct. Aqueous Formic Acid 10 Pct. Formic Acid 100 Pct. Formic Acid 25 Pct. | E E U E U E | E L U G U G | — U — U U — | — U — U U — |
| Formic Acid 3 Pct. Formic Acid 50 Pct. Freon-12 Fructose Fruit Pulps and Juices Fuel Oil | E L E E E G | G U G E E L | U U E E E E | U U E E E E |
| Furfural Furfuryl Alcohol Gallic Acid Gas-Coke Oven Gas-Manufactured Gas-Natural (Dry) | U E E G U E | U L E G U E | U — — G — E | U — — G — E |
| Gas-Natural (Wet) Gasoline Gasoline – Refined Gasoline – Sour Gelatine Gin | E U L L E E | E U U U E G | E — E E E — | E — G G E — |
| Ginger Ale Glucose Glycerine (Glycerol) Glycol Glycolic Acid 30 Pct. Grade Sugar | E E E E E — | E E E E E — | — E E G U — | — E E G U — |
| Grape Juice Grapefruit Juice Grease Green Liquor (Paper industry) Heptachlor Heptane | E E E E E L | E E L E L U | — — — — — E | — — — — — — |
| Hexadecanol Hexane Hexanol, Tertiary Honey Hydrochloric Acid 10 Pct. Hydrochloric Acid 48 Pct. | — L L E E E | — U U E E L | — — G — U U | — — — — U U |
| Hydrocyanic Acid 10 Pct. Hydrofluoric Acid 10 Pct. Hydrofluoric Acid 4 Pct. Hydrofluoric Acid 48 Pct. Hydrofluoric Acid 60 Pct. Hydrofluoroboric Acid | — G G G G E | — L G U U E | — U U U U — | — U U U U — |
| Hydrofluorosilic Acid Hydrogen Hydrogen Bromide (Dry) Hydrogen Chloride (Dry) (Liquid) Hydrogen Cyanide Hydrogen Peroxide 3 –12 Pct. | G E — — E E | L G — — E G | U E — E U — | U E — E U — |
| Hydrogen Peroxide 30 Pct. Hydrogen Peroxide 50 Pct. Hydrogen Peroxide 90 Pct. Hydrogen Phosphide Hydrogen Sulfide – Aqueous Solution Hydrogen Sulfide – Dry | E E U E E E | G L U L E E | G L U — — — | L U U — — — |
| Hydrombromic Acid 20 Pct. Hydroquinone Hydroxylamine Sulfate Hypochlorous Acid Inks Iodine (In Alcohol) | E E E E — U | G E E E — U | U E — L — U | U E — U — U |
| Iso-octane Isopropyl Acetate Isopropyl Alcohol Jelly | G U E E | L U G E | — — — — | — — — — |

Key: E — Excellent	G — Good	L — Limited	U — Unsatisfactory

PVC and Polyurethane Chemical Resistance Guide

| Material Handled | Hose Materials of Construction and Temperatures |  |  |  |
| --- | --- | --- | --- | --- |
|  | PVC |  | Thermoplastic Polyurethane |  |
|  | 68°F | 104°F | 68°F | 104°F |
| Jet Fuels JP 3,4,5 Kerosene Ketones Kraft Liquor (Paper industry) Lacquer Thinners Lactic Acid 28 Pct. | U U U E L E | U U U E U E | G E — — G U | L G — — — U |
| Lard (marginal) Lard Oil Lauric Acid Lauryl Chloride Lauryl Sulfate Lead Acetate | G E E E E E | L G E E E E | — E L E — E | — G U G — E |
| Lead Arsenate Lead Nitrate Lead Tetra-ethyl Lemon Juice Lime Sulfur Linoleic Acid | — — — E E E | — — — G E E | — — — — — L | — — — — — U |
| Linseed Oil Liquors (Chemical) Lubricating Oils Magnesium Carbonate Magnesium Chloride Magnesium Hydroxide | E E U E E E | E G U E E E | E — E E G G | E — E E L L |
| Magnesium Nitrate Magnesium Sulfate Maleic Acid 25 Pct. Aqueous Maleic Acid 50 Pct. Maleic Acid Concentrated Malic Acid | E E E — — E | E E E — — E | E E L — — L | E E U — — U |
| Manganese Suphate Mayonnaise Mercuric Chloride Mercuric Cyanide Mercurous Nitrate Mercury | — E G G G G | — E G G G G | — — G — G — | — — L — G — |
| Metallic Soaps Methyl Acetate Methyl Alcohol Methyl Bromide Methyl Chloride Methyl Ethyl Ketone | — U L U U U | — U U U U U | — — L — U L | — — U — U U |
| Methyl lsobutyl Ketone Methyl Sulfate Methyl Sulfuric Acid Methylated Spirit Methylene Chloride Milk | U E E — U E | U G E — U E | — E U — U — | — G U — U — |
| Mineral Oils Mineral Spirits Molasses Monochlorobenzene Naphtha Napthalene | E — E U U L | G — E U U U | E — E — E — | E — E — E — |
| Nickel Acetate Nickel Chloride Nickel Nitrate Nickel Sulphate Nicotine Nicotine Acid | E E E E E E | E E E E E G | E E E E E L | E E E E E U |
| Nitric Acid (Anhydrous) Nitric Acid 10 Pct. Nitric Acid 25 Pct. Nitric Acid 35 Pct. Nitric Acid 40 Pct. Nitric Acid 50 Pct. | U E G G G — | U G L L L — | U U U U U — | U U U U U — |
| Nitric Acid 60 Pct. Nitric Acid 68 Pct. Nitric Acid 70 Pct. Nitrobenzene Nitrous Oxide Oats | G L U U E E | U U U U E U | U U — U E — | U U — U E — |
| Octyl Alcohol Oils and Fats Oils, Petroleum Oleic Acid | — E E G | — G G L | — E E U | — E E U |

| Material Handled | Hose Materials of Construction and Temperatures |  |  |  |
| --- | --- | --- | --- | --- |
|  | PVC |  | Thermoplastic Polyurethane |  |
|  | 68°F | 104°F | 68°F | 104°F |
| Oleum Olives Orange Juice Oxalic Acid Oxygen Ozone | U E E E E L | U E E E E U | U — — U E — | U — — U E — |
| Palmitic Acid 10 Pct. Palmitic Acid 70 Pct. Paraffin Peaches Peanut Butter Peas | E L E E E E | G U G E G E | U U — — — — | U U — — — — |
| Pentachlorophenol in Oil Pentane Peracetic Acid 40 Pct. Perchloric Acid 10 Pct. Perchloric Acid 70 Pct. Perchlorethylene | G G U G L U | L U U L U U | — — U U U — | — — U U U — |
| Petrol Petroleum Ether Phenol Phenylhydrazine Phenylhydrazine Hydrochloride Phosgene (Gas) | U L U U L E | U L U U U G | — — U — — — | — — U — — — |
| Phosgene (Liquid) Phosphoric Acid — 0-25 Pct. Phosphoric Acid — 25-50 Pct. Phosphoric Acid — 50-90 Pct. Phosphorus (Yellow) Phosphorus Pentoxide | U E E E G U | U E E E L U | — U U U — — | — U U U — — |
| Phosphorus Trichloride Photographic Chemicals Photographic Developers Photographic Emulsions Photographic Fixers Picric Acid | U E — — — U | U E — — — U | — E — — — U | — G — — — U |
| Pineapple Juice Pitch Plating Solutions Brass Cadmium Chromium | E G — E E G | E L — E E G | — — — E E G | — — — E E G |
| Copper Gold Judium Lead Nickel Rhodium | E E E E E E | E E E E E E | E E E E E E | E E E E E E |
| Silver Tin Zinc Potassium Acid Sulfate Potassium Antimonate Potassium Bicarbonate | E E E E E E | E E G E E E | E E E E E E | E E E E E E |
| Potassium Bichromate Potassium Bisulfite Potassium Bisulphate Potassium Borate 1 Pct. Potassium Bromate 10 Pct. Potassium Bromide | E E — E E E | E E — E E E | E E — E E E | E E — E E E |
| Potassium Carbonate Potassium Chlorate Potassium Chloride Potassium Chromate 40 Pct. Potassium Cuprocyanide Potassium Cyanide | E E E E E E | E E E E E E | E G E G — E | E G G G — E |
| Potassium Dichromate 40 Pct. Potassium Ferricyanide Potassium Fluoride Potassium Hydroxide 10 Pct. Potassium Hydroxide 20 Pct. Potassium Hydroxide 35 Pct. | E E E E E E | E E E E E E | G E E L U U | G E G U U U |
| Potassium Hydroxide Conc. Potassium Hypochlorite Potassium Nitrate Potassium Perborate | — G E E | — L E E | — U E E | — U E E |

Key: E — Excellent	G — Good	L — Limited	U — Unsatisfactory

PVC and Polyurethane Chemical Resistance Guide

| Material Handled | Hose Materials of Construction and Temperatures |  |  |  |
| --- | --- | --- | --- | --- |
|  | PVC |  | Thermoplastic Polyurethane |  |
|  | 68°F | 104°F | 68°F | 104°F |
| Potassium Perchlorite Potassium Permanganate 10 Pct. Potassium Persulfate Potassium Phosphate Potassium Sulfate Potassium Sulfide | E G E — E E | E G E — E E | G G E — E E | L L E — E E |
| Potassium Thiosulfate Potatoes Propane Propargyl Alcohol Propyl Alcohol Propylene Dichloride | E E E E E U | E E E E L U | E — E — G U | E — E — L U |
| Propylene Glycol Prune Juice Raisins Ritchfield "A" Weed Killer Salicylic Acid Salt Water | U E E E — E | U E E L — E | U — — — — G | U — — — — U |
| Selenic Acid Shortening Silicic Acid Silicone Fluids Silver Cyanide Silver Nitrate | E G E — E E | G L E — E E | U — U — E E | U — U — E E |
| Silver Plating Solutions Soap Solution Soda Sodium Acetate Sodium Acid Sulfate Sodium Aluminate | E E E E E — | G E E E E — | E G — E E — | E U — E E — |
| Sodium Antimonate Sodium Arsenite Sodium Benzoate Sodium Bicarbonate Sodium Bisulfate Sodium Bisulfite | E E E E E E | E E G E E E | E E E E E E | E E E E E E |
| Sodium Bromide Sodium Carbonate (Soda Ash) Sodium Chlorate Sodium Chloride Sodium Cyanide Sodium Dichromate | E E G E E E | E E L E E G | E E G E E E | G E G G E G |
| Sodium Ferricyanide Sodium Ferrocyanide Sodium Fluoride Sodium Hydroxide 10 Pct. Sodium Hydroxide 35 Pct. Sodium Hydroxide 50 Pct. | E E E L U U | E E E L U U | E E E L U — | E E G U U — |
| Sodium Hydroxide Saturated Sodium Hypochlorite Sodium Nitrate Sodium Nitrite Sodium Phosphate-Acid Sodium Silicate | E E E E G E | E E E E G E | U U E E U E | U U E E U E |
| Sodium Sulfate Sodium Sulfide Sodium Sulfite Sodium Thisulfate (Hypo) Soya Beans Soya Oil | E E E E E E | E E E E U G | E E E E — — | E E E G — — |
| Soybean Oil Spinach Squash Stannic Chloride Stannous Chloride Starch | E E E E E — | E E E E G — | — — — E E — | — — — G G — |
| Stearic Acid Stoddard Solvent Styrene Sucrose Sugar (All Forms) Sulfur | E L U — E G | G U U — E G | L G — — — — | U G — — — — |
| Sulfuric Acid 0-10 Pct. Sulfuric Acid 10-40 Pct. Sulfuric Acid 50-60 Pct. Sulfuric Acid 70 Pct. | E E E E | G G G G | L U U U | U U U U |

| Material Handled | Hose Materials of Construction and Temperatures |  |  |  |
| --- | --- | --- | --- | --- |
|  | PVC |  | Thermoplastic Polyurethane |  |
|  | 68°F | 104°F | 68°F | 104°F |
| Sulfuric Acid 95 Pct. Sulfuric Acid 95 Pct. to Fuming Sulfurous Acid Sulphur Dioxide Gas-Dry Sulphur Dioxide Gas-Wet Sulphur Dioxide-Liquid | U L G E U L | U L L E U U | U U U — — — | U U U — — — |
| Sulphur Trioxide Sulphurous Acid 10 Pct. Sulphurous Acid 30 Pct. Tall Oil Tallow Tannic Acid | E — — U — E | G — — U — E | — — — — — L | — — — — — U |
| Tanning Extracts Tanning Liquors Tartaric Acid Tea (Brewed) Tetraethyl Lead Tetrahydrofurane | — E E E G U | — E G E L U | — — L — G U | — — U — G U |
| Tetrahydronaphihalene Thionyl Chloride Tin Chloride Titanium Tertachloride Titanium Trichloride Toluol or Toluene | — U E E — U | — U E U — U | — U E L — L | — U E U — U |
| Tomato Juice Tomato Puree & Paste Tomatoes Transformer Oil Tributyl Phosphate Trichlorobenzene | E E E — U — | E E E — U — | — — — — — — | — — — — — — |
| Trichloroethylene Tricresyl Phosphate Triethanolamine Triethylamine Trimethyl Propane Trisodium Phosphate | U U L G L E | U U U L U E | L U — — — E | U U — — — E |
| Turpentine Urea Urine Vanilla Extract Varnish Vegetable Oils | L E E — U G | U G E — U L | E E E — E — | G E E — G — |
| Vinegar Vinyl Acetate Vinyl Chloride Vodka Water-Acid Mine Water Water-Distilled | E U U E E E | G U U G E E | G U — — G G | L U — — U U |
| Water-Fresh Water-Salt Wetting Agents Whey Whiskey White Gasoline | E E — — E E | E E — — G E | G G — — — E | U U — — — G |
| White Liquor (Paper industry) Wines Xylene or Xylol Yeast Yogurt Zinc Chloride | E E U E E E | E G U U G E | — — G — — E | — — L — — E |
| Zinc Chromate Zinc Cyanide Zinc Nitrate Zinc Sulfate | E E E E | E E E E | E E E E | E E E E |
| Mixtures of Acids: Nitric 15 Pct., Hydrofluoric 4 Pct. Sodium Dichromate 13 Pct., Nitric Acid 16 Pct., Water 71 Pct. | E E | G G | U U | U U |

Key: E — Excellent	G — Good	L — Limited	U — Unsatisfactory

Key: G — Good	L — Limited	U — Unsatisfactory

Material Handled

68˚F 104˚F

Material Handled

68˚F 104˚F

Material Handled

68˚F 104˚F

EPDM Chemical Resistance Guide

Acetic Acid	G	G

Acetone	G	G

Aluminum Acetate	G	G

Aluminum Chloride	G	G

Aluminum Hydroxide	G	G

Aluminum Sulfate	G	G

Ammonia (Gas)	G	G

Ammonia (Liquid)	G	G

Ammonium Acetate (Conc.)	G	G

Ammonium Chloride	G	G

Ammonium Hydroxide	G	G

Ammonium Nitrate	G	G

Aniline	L	L

Aniline Sulfate	U	U

Barium Chloride	G	G

Barium Hydroxide	G	G

Beer	G	G

Benzen Alcohol	L	L

Benzene	U	U

Bromine	U	U

Butyl Alcohol	L	L

Calcium Carbonate	G	G

Calcium Chloride (Conc.)	G	G Calcium Hyprocholite (Conc.)L	L

Carbon Monoxide	G	G

Carbon Tetrachloride	L	L

Carbonic Acid	G	G

Carbonic Acid Gas	G	G

Cetyl Alcohol	L	L

Chlorine	- 10% Gas	L	L

- 100% Gas	L	L

(Solution)	L	L

Chloroform	U	U

Chromate (Plating Solution)	L	L

Citric Acid	G	G

Copper Chloride	G	G

Copper Nitrate	G	G

Copper Sulfate	G	G

Creosote Oil	U	U

Development Sol.	L	L

Dextrin	G	G

Dichlorethylene	U	U

Dichloro Benzene	U	U

Diethyl Ether	G	G

Emulsifier	G	G

Ether	G	G

Ethyl Acetate	L	L

Ethyl Alcohol - 6%	G	G

- 100%	G	G

Ethylene Chloride	L	L

Ethylene Glycol	G	G

Fluorine	U	U

Glycerol	G	G

Grape Sugar	G	G

Hormamide- 40%	G	G

Hydrochloric Acid - 10%	G	L

- 20%	G	L

Concentrate	G	L

Hydrogen	G	G

Hydrogen Chloride (Anhydrous)	G	L Hydrogen Peroxide - 3%	U	U

- 30%	U	U

(Above 80%)	U	U

Hydrogen Sulfide	G	G

Iodine	U	U

Iron Chloride	G	G

Iron Sulfate	G	G

Isopropyl Alcohol	G	G

Magnesium Carbonate	G	G

Magnesium Chloride	G	G

Magnesium Hydroxide	G	G

Magnesium Sulfate	G	G

Methanol - 20%	G	G

Monochloro Benzene	U	U

Nitric Acid	- 5%	L	L

- 50%	L	L

- 70%	U	U

- 95%	U	U

Oleic Acid	L	L

Ozone	G	G

Parraffin	U	U

Perchlorethylene	U	U

Phenol	L	L

Phosphoric Acid - 30%	G	G

Photosensitive Emulsion	G	G

Potassium Bichromate	U	U

Potassium Bromide	G	G

Potassium Chloride	G	G

Potassium Cyanide	G	G

Potassium Fluoride	G	G Potassium Hydroxide - 10%	G	G

(Conc.)	G	G

Potassium Permanganate	U	U

Potassium Phosphate	G	G

Propylene Glycol	G	G

Sake (Alcohol)	G	G

Salt Water	G	G

Sauce	G	G

Sodium Bicarbonate	G	G

Sodium Chloride	G	G

Sodium Hydroxide - 10%	G	G

(Conc.)	G	G

Sodium Hypoclorite - 15%	G	G

Soy Sauce	G	G

Stearic acid	L	L

Sulfur Dioxide	U	U

Sulfuric Acid	L	L

Methyl Alcohol- 6%

- 100%

Methyl Ethel Ketone Methylene Chloride Mineral Oil

G G G L U

G G G L U

Sulfurous Acid - 30%	L	L

Tetrahydrofuron	L	L

Toluene	U	U

Transformer Oil	U	U

Water	G	G

Zinc Chloride	G	G

SBR Chemical Resistance Guide

Ethylene Glycol G

Fluorine U

Formaldehyde (40%) L

Glycerol G

Grape Sugar G

| Potassium Bichromate | U |
| --- | --- |
| Potassium Bromide | G |
| Potassium Chloride | G |
| Potassium Cyanide | G |
| Potassium Fluoride | G |

Hydrogen Peroxide (3%) U

Hydrogen Peroxide (30%) U

Hydrogen Peroxide (80% or more) U

Hydrogen Sulfide U

Iodine U

| Sake | G |
| --- | --- |
| Salt Water | G |
| Sodium Bicarbonate | G |
| Sodium Chloride | G |
| Sodium Hydroxide (10%) | G |

Creosote Oil U

Dextrin G

Dichlorobenzene U

Dichloromethane U

Diethyl Ether U

| Nitric Acid (70%) | U |
| --- | --- |
| Nitric Acid (95%) | U |
| Nitrous Acid (10%) | L |
| Oleic Acid | U |
| Oxalic Acid | L |

Key: G — Good	L — Limited	U — Unsatisfactory

| Material Handled 68ºF Material Handled 68ºF Material Handled 68ºF |  |  |
| --- | --- | --- |
| 1,1-dichloroethylene U 1,2-dichloroethane U Acetic Acid (10%) L Acetone L Aluminum Acetate L Aluminum Chloride G Aluminum Hydroxide G Aluminum Sulfide L Ammonia (Gas) G Ammonia (Liquid) G Ammonium Acetate (Conc.) G Ammonium Bicarbonate G Ammonium Chloride G Ammonium Hydroxide U Ammonium Nitrate G Aniline U Aniline Sulfate U Barium Chloride G Barium Hydroxide G Beer L Benzene U Benzyl Alcohol U Bromine U Butyl Alcohol G Calcium Carbonate G Calcium Chloride (Conc.) G Calcium Chloride (in 20% Mesh) G Calcium Hypochlorite (15% Cl2) U Calcium Hypochlorite (Conc.) U Carbon Dioxide U Carbon Monoxide L Carbon Tetrachloride U Carbonic Acid L Carbonic Acid Gas G Cetyl Alcohol L Chlorine (10% Gas) U Chlorine (100% Gas) U Chlorine (Solution) U Chloroform U | Chromate (25%) U Citric Acid G Copper Chloride G Copper Nitrate G Copper Sulfate L Emulsifier G Ether L Ethyl Acetate U Ethyl Alcohol (100%) G Ethyl Alcohol (6%) G Hydrochloric Acid (10%) L Hydrochloric Acid (20%) L Hydrochloric Acid (Conc.) L Hydrogen L Hydrogen Chloride (Anhydride) L Iron Chloride G Iron Sulfate G Isopropyl Alcohol L Magnesium Carbonate G Magnesium Chloride G Magnesium Hydroxide L Magnesium Sulfate L Methyl Alcohol (100%) G Methyl Alcohol (6%) G | Methyl Ethyl Ketone (MEK) U Mineral Oil U Monochlorobenzene U Nitric Acid (5%) U Nitric Acid (50%) U Ozone U Paraffin U Perchloroethylene U Phenol U Phosphoric Acid (30%) U Potassium Hydroxide (10%) L Potassium Hydroxide (Conc.) L Potassium Permanganate U Potassium Sulfate G Propylene Glycol L Sodium Hydroxide (Conc.) G Soy Sauce G Stearic Acid L Sulfuric Acid (10%) U Tetrahydrofuran U Toluene U Transformer Oil U Water G Zinc chloride G |

Company Profile

Company Name 				Contact		 Address 		City 			State 	Zip	 Phone 	Fax 			E-mail

Application Details

Application

Indoor ❏  Outdoor ❏

Material conveyed 	Solid ❏  Liquid ❏  Gas ❏

Type of fittings to be used

Hose Construction

Hose style:

  - Smooth profile (e.g. F series): ❏

  - Convoluted profile (e.g. W series): ❏

  - Externally reinforced (e.g. GT series): ❏

  - Other: ❏ Describe  	 Similar to existing Tigerflex™ hose part number(s) (if applicable)

Flex material  	 Helix material

Flex color  	 Helix color

Food Grade? Yes ❏ No ❏

Food Grade? Yes ❏ No ❏

Tigerflex™ Products Custom Inquiry Form

Yarn reinforcement? Yes ❏ No ❏	Polyurethane liner? Yes ❏ No ❏	Grounding wire? Yes ❏ No ❏

Hose size(s) (ID)   				 Required working pressure 	PSI @ 68º F	Required vacuum rating 	in/g @ 68º F

Required bending radius 	in	Required hose weight 		lbs Hose Length 		ft	Tolerance +/- 	in

Approvals required?  	 Other requirements

Delivery Information

Estimated annual volume 	Reoccurring? Yes ❏  No ❏	Required ship date  	                   Special packaging or shipping requirements

Submit to:

Fax: (847) 885-9010 • Email: customerservice@kuriyama.com • Submission date

75

For Over 50 Years THE KURIYAMA VALUE

Innovative and Effective Application Solutions

kuriyama.com/50years

# Cautionary Statement

All Products sold and distributed by Kuriyama of America, Inc. are in the nature of commodities and they are sold by published specifications and not for particular purposes, uses or applications. Purchaser shall first determine their suitability for the intended purposes, uses or applications and shall either conduct its own engineering studies or tests, or retain qualified engineers, consultants or testing laboratories and consult with them before determining the proper use, suitability or propriety of the merchandise or Products for the intended purposes, uses or applications.

Kuriyama of America, Inc. (“Seller”) does not recommend the Products for any particular purpose, use or application, and the Purchaser or user thereof shall assume full responsibility for the suitability, propriety, use and application of the Products. Purchaser shall follow all instructions contained in Seller’s catalogs, brochures, technical bulletins and other documents regarding the Products. The Products, including but not limited to, hose, tubing or couplings, may fail due to the use or conveyance of substances at elevated or lowered temperatures or at excessive pressure, the conveyance of abrasive, injurious, flammable, explosive or damaging substances.

Hose or tubing used in bent configurations will be subjected to increased abrasion. Hose clamps or couplings may loosen after initial installation and all sections of hose and tubing including connections, couplings, clamps, con- ductivity and bonding should be inspected frequently, regularly and consistently, and should be replaced, adjusted or re-tightened for the avoidance of leakage, for the prevention of injuries or damages, and for general safety purposes. Except as indicated in its Limited Warranty, Seller shall not be liable or responsible for direct or indirect injuries or damages caused by or attributed to the failure or malfunction of any Products sold or distributed by it.

Purchasers or users of the Products should frequently and consistently undertake inspections and protective measures with respect to the use and application of Products, which should include the examination of tube and cover, conditions of the hose or tubing, and the identification, repair or replacement of sections showing cracking, blistering, separations, internal and external abrasions, leaking or slipped couplings or connections and make proper proof tests.

# Limited Warranty

The Products sold or distributed by Seller are warranted to its customers to be free from defects in mate- rial and workmanship at the time of shipment by us, subject to the following provisions. ALL WARRANTY CLAIMS SHALL BE MADE WITHIN SIX (6) MONTHS AFTER SELLER SHIPPED THE PRODUCTS. SELLER’S LIABILITY HEREUNDER IS LIMITED AT SELLER’S EXCLUSIVE DISCRETION, TO 1) THE PURCHASE PRICE OF ANY PRODUCTS PROVING DEFECTIVE; 2) REPAIR OF ANY DEFECTIVE PRODUCT OR PART THEREOF; OR 3) REPLACEMENT OF ANY DEFECTIVE PRODUCT OR PART UPON ITS AUTHORIZED RETURN TO SELLER.

THIS WARRANTY IS IN LIEU OF AND EXCLUDES ALL OTHER WARRANTIES, EXPRESSED, IMPLIED, STATUTORY, OR OTHERWISE CREATED UNDER APPLICABLE LAW INCLUDING, BUT NOT LIMITED TO, THE WARRANTY OF MERCHANTABILITY AND THE WARRANTY OF FITNESS FOR A PARTICULAR PURPOSE. IN NO EVENT SHALL SELLER OR THE MANUFACTURER OF THE PRODUCT BE LIABLE FOR SPECIAL, INCIDENTAL, OR CONSEQUEN- TIAL DAMAGES, INCLUDING LOSS OF PROFITS, WHETHER OR NOT CAUSED BY OR RESULTING FROM THE NEGLIGENCE OF SELLER AND/OR THE MANUFACTURER OF THE PRODUCT, UNLESS SPECIFICALLY PROVIDED HEREIN. IN ADDITION, THIS WARRANTY SHALL NOT APPLY TO ANY PRODUCTS OR PORTIONS THEREOF WHICH HAVE BEEN SUBJECTED TO ABUSE, MISUSE, IMPROPER INSTALLATION, MAINTENANCE, OR OPERATION, ELECTRICAL FAILURE OR ABNORMAL CONDITIONS, AND TO PRODUCTS WHICH HAVE BEEN TAMPERED WITH, ALTERED, MODIFIED, REPAIRED, REWORKED BY ANYONE NOT APPROVED BY SELLER, OR USED IN ANY MANNER INCONSISTENT WITH THE PROVISIONS OF THE “CAUTIONARY STATEMENT” ABOVE OR ANY INSTRUCTIONS OR SPECIFICATIONS PROVIDED WITH OR FOR THE PRODUCT.

09/2005

Distributed by:

#### CONTACT OUR SALES/WAREHOUSE LOCATIONS BELOW WHICH SERVE YOUR AREA

SOUTHWEST WAREHOUSE KURIYAMA OF AMERICA, INC.

HOUSTON

200 PORTWALL STREET, SUITE 100

HOUSTON, TX 77029

Phone: (713) 674-8212

Toll Free Phone: (800) 501-6808

FAX: (713) 674-5214

Toll Free FAX: (800) 800-5214

E-Mail: sales@kuriyama.com

WESTERN WAREHOUSE KURIYAMA OF AMERICA, INC.

SANTA FE SPRINGS

10749 SHOEMAKER AVENUE SANTA FE SPRINGS, CA 90670-4039 Phone: (562) 941-4507

FAX: (562) 941-8940

Toll-Free FAX: (800) 326-8940

E-Mail: sales@kuriyama.com

SOUTHEAST WAREHOUSE FORTNEY SALES CO., INC. 4221 CANTRELL ROAD NW ACWORTH, GA 30101

PHONE: (770) 427-6528

FAX: (770) 423-9249

Toll Free FAX: (800) 423-9249

Web Site: www.fortneysales.com E-Mail: sales@fortneysales.com

EASTERN WAREHOUSE

EASTERN RUBBER & PLASTICS CO., INC.

100 GOLDMAN DR. PLUMSTED INDUSTRIAL PARK CREAM RIDGE, NJ 08514 Phone: (609) 758-0100

FAX: (609) 758-0102

Toll Free FAX: (800) 445-7138

Web Site: www.easternrubber.com E-Mail: sales@easternrubber.com

#### IN CANADA:

KURI TEC CORPORATION

140 ROY BOULEVARD

BRANTFORD, ON, CANADA N3R 7K2 Phone: (519) 753-6717

FAX: (519) 753-7737

Web Site: http://www.kuritec.com E-Mail: sales@kuritec.com

#### IN MEXICO:

KURIYAMA DE MÉXICO S DE RL DE CV AV JOSE PALOMO MARTINEZ NO 520-20 BODEGA 5

PARQUE INDUSTRIAL OMOLAP APODACA, N.L. CP:66633, MÉXICO

Telefonos: (81) 1086-1870 O 71

Lada sin Costo 01 800 822 52 00

FAX: (81) 1086-1869

Internet: www.kuriyama.com

Correo Electronico: ventas@kuriyama.com

Headquarters, Sales Office and Warehouse Location

360 E. State Parkway, Schaumburg, IL 60173-5335 Phone: (847) 755-0360 • Toll-free FAX: (800) 800-0320

International FAX: (847) 885-0996

Web Site: http://www.kuriyama.com

E-Mail: sales@kuriyama.com

			kuriyama.com/50years

THE ASSOCIATION FOR HOSEAND ACCESSORIES DISTRIBUTION

©2019 Kuriyama of America, Inc. All rights reserved.	4.5M   02/19	Printed in U. S. A.	KTFCA0219